Crystal Structure Report for L. Dalton

Submitted by Brenden Carlson

Sample ID - napPhPhen

by Werner Kaminsky

X-ray Crystallography Laboratory

University of Washington

21. January 2003

Data backup accessibly through ftp:

computer: 		chmraypc.cpac.washington.edu

login: 		anonymous

password:		(your name or email address)

location: 	c:\structures\dalton\brenden\NapPhPhen

Data backup accessibly through http:

URL: 	http://cad4.cpac.washington.edu/structures

Username: 	xray-user

Password: 	hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@wintensor.com

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A clear crystal plate size 0.20 x 0.60 x 0.0.02 mm was mounted on a glass capillary with oil.  Data was collected at -143oC with one set of exposure as follows:

Scan 		Type	Scanlength (deg.)  start (deg.)	(     	(	(     	(

1	      	(        	182.0					3.70	-1.5	160  	 0

Crystal-to-detector distance was 30 mm and exposure time was 20 seconds per degree for all sets.  The scan width was 1o.   Data collection was 81.4% complete to 23.36o in (.  A total of  12677 partial and complete reflections were collected covering the indices, h = -6 to 7, k = -7 to 7,  l = -23 to 26.  1654 reflections were symmetry independent and the Rint = 0.086 indicated that the data was of slightly less than average quality (0.07).

Indexing and unit cell refinement were inconclusive. (several other datasets did not lead to a better result) Data was solved in P1.

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S = exp(2B(sinq/()2)/ scale

S is calculated from the scale and the B factor is determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS97) produced a complete heavy atom phasing model with motivs of the proposed structure. A nonidentified solvent molecule was found

The data did not result in a publishable structure. The plot below summarizes all that is available.