Crystal Structure Report for

Satheeshkumar Rajendran

by Werner Kaminsky

ID – 2SClA

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 5/6/2015

Documentation finished: 6/11/2015

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A colorless prism, measuring 0.40 x 0.20 x 0.15 mm3 was mounted on a loop with oil.  Data was collected at -143oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 35 mm and exposure time was 30 seconds per degree for all sets.  The scan width was 1.3o.   Data collection was 99.6% complete to 25o  in .  A total of  6876 merged reflections were collected covering the indices, h = -11 to 11, k = -20 to 21,  l = -30 to 30.  3682 reflections were symmetry independent and the Rint = 0.0541 indicated that the data was of better than average quality (0.07).  Indexing and unit cell refinement indicated a primitive orthorhombic lattice.  The space group was found to be P b c a  (No.61).

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C19 H13 Cl F N O

Formula weight 	325.75

Temperature 	130(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P b c a

Unit cell dimensions	a = 8.3730(2) Å	= 90°.

b = 15.3447(4) Å	= 90°.

c = 23.1401(9) Å	 = 90°.

Volume	2973.07(16) Å3

Z	8

Density (calculated)	1.456 Mg/m3

Absorption coefficient	0.271 mm-1

F(000)	1344

Crystal size	0.40 x 0.20 x 0.15 mm3

Theta range for data collection	2.80 to 28.33°.

Index ranges	-11<=h<=11, -20<=k<=20, -30<=l<=30

Reflections collected	6876

Independent reflections	3682 [R(int) = 0.0541]

Completeness to theta = 25.00°	99.6 %

Max. and min. transmission	0.9604 and 0.8992

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3682 / 0 / 208

Goodness-of-fit on F2	0.946

Final R indices [I>2sigma(I)]	R1 = 0.0493, wR2 = 0.1126

R indices (all data)	R1 = 0.0967, wR2 = 0.1291

Largest diff. peak and hole	0.552 and -0.325 e.Å-3

Otwinowsky, Z.; Minor, W. In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 1997, 276, 307-326.

(a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.

Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565