Crystal Structure Report for K.SARAVANA MANI

by Werner Kaminsky

Sample ID – 68DMPRSP

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 8/2/2016

Documentation finished: 8/8/2016

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A colorless plate, measuring 0.25 x 0.20 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at 21oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 30 mm and exposure time was 200 seconds per degree for all sets.  The scan width was 2o.   Data collection was 99.4% complete to 25o  in .  A total of  12177 partial and complete reflections were collected covering the indices, -11<=h<=12, -15<=k<=15, -18<=l<=18.  7275 reflections were symmetry independent and the Rint = 0.0769 indicated that the data was of average quality.  Indexing and unit cell refinement indicated a triclinic P lattice.  The space group was found to be P1  (No.2).

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C39 H30 Cl N4 O

Formula weight 	606.12

Temperature 	294(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 9.7080(12) Å	= 91.344(7)°.

b = 11.5722(15) Å	= 99.494(7)°.

c = 14.215(2) Å	 = 106.741(7)°.

Volume	1504.1(3) Å3

Z	2

Density (calculated)	1.338 Mg/m3

Absorption coefficient	0.167 mm-1

F(000)	634

Crystal size	0.25 x 0.20 x 0.05 mm3

Theta range for data collection	2.23 to 28.32°.

Index ranges	-11<=h<=12, -15<=k<=15, -18<=l<=18

Reflections collected	12177

Independent reflections	7275 [R(int) = 0.0769]

Completeness to theta = 25.00°	99.4 %

Max. and min. transmission	0.9917 and 0.9594

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7275 / 0 / 409

Goodness-of-fit on F2	0.897

Final R indices [I>2sigma(I)]	R1 = 0.0562, wR2 = 0.1237

R indices (all data)	R1 = 0.1646, wR2 = 0.1649

Extinction coefficient	0.0127(19)

Largest diff. peak and hole	0.359 and -0.269 e.Å-3

Otwinowsky, Z.; Minor, W. In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 1997, 276, 307-326.

(a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565