Crystal Structure Report for D. Xiao

By Paige M Gannon & Werner Kaminsky

Sample Submitted by Austin Kamin

ID – AAK_4178_1

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 6/6/2022

Documentation finished: 6/9/2022

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A gray flake, measuring 0.xx x 0.xx x 0.xx mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 60 seconds per frame for all sets.  The scan width was 0.75o.   Data collection was 100% complete to 25o in .  A total of  16692 reflections were collected covering the indices, -12<=h<=12, -16<=k<=16, -21<=l<=21.  8358 reflections were symmetry independent and the Rint = 0.1554 indicated that the data was apprpriate.  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P1  (No. 2).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure shows two half complexes completed by symmetry, one of which being disordered. In addition, two disordered BF4 anions were observed.

The structure is of high quality and ready for publication (I lowered the theta-max slightly below 25 degrees, leading to a C-level warning in checkcif, but removing a B-warning this way which I believe is beneficial – let me know if you encounter any problem during submission to a journal).

Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Identification code 	AAK_4178_1

Empirical formula 	C54 H46 B2 F8 Fe2 N8 O4

Formula weight 	1156.31

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 10.5990(10) Å	a= 83.672(7)°.

b = 13.9435(15) Å	b= 74.388(7)°.

c = 18.859(2) Å	g = 71.152(7)°.

Volume	2539.6(5) Å3

Z	2

Density (calculated)	1.512 Mg/m3

Absorption coefficient	0.657 mm-1

F(000)	1184

Crystal size	0.140 x 0.080 x 0.030 mm3

Theta range for data collection	1.544 to 24.405°.

Index ranges	-12<=h<=12, -16<=k<=16, -21<=l<=21

Reflections collected	16692

Independent reflections	8358 [R(int) = 0.1554]

Completeness to theta = 24.405°	100.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8358 / 312 / 808

Goodness-of-fit on F2	0.932

Final R indices [I>2sigma(I)]	R1 = 0.0641, wR2 = 0.1055

R indices (all data)	R1 = 0.1935, wR2 = 0.1409

Largest diff. peak and hole	0.417 and -0.486 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,  Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565