Crystal Structure Report for A. Velian

by Dylan Rogers & Werner Kaminsky

Sample Submitted by Andrei Chirila

ID – ACH_063

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 7/19/18

Documentation finished: 7/23/18

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A black prism, measuring 0.20 x 0.14 x 0.12 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.5% complete to 25o  in .  A total of  19157 reflections were collected covering the indices, -26<=h<=26, -19<=k<=20, -16<=l<=36.  9777 reflections were symmetry independent and the Rint = 0.0472 indicated that the data was of better than average quality (0.07).  Indexing and unit cell refinement indicated a C-centered monoclinic lattice.  The space group was found to be C 2/c  (No.15).

The data appeared twinned via 180 degrees about (0 0 1) of the Niggly (reduced) cell (12.618 Å, 12.618 Å, 26.797 Å, 99.57º, 100.3º, 105.5º); transformation from C-centered monoclinic to reduced cell: (-0.5 -0.5 0, 0.5 -0.5 0, 0.5 0.5 1), reduced to C-centered cell: (-1 1 0,  -1 -1 0,  1 0 1) (CELL_NOW) and after multi-domain integration (SAINT, SADABS within the APEX2 software package by Bruker) the data was merged utilizing twinabs.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The asymmetric unit contains a disordered ethyl ether solvent and a half of a chemically disordered cluster complex, with one component at 87% containing Cu, the other at 13% lacking the Cu(II) but showing the nitrogen protonated. The complex is completed by a two-fold axis. Additional structural disorder includes split nitrogen positions resulting from the presence versus absence of the Cu and protonation in the other case.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

a)

b)

Figure 1a) ORTEP of the cluster complex containing Cu, b) protonated nitrogen, with thermal ellipsoids at the 50% probability level. Some disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C62 H114.25 Co6 Cu0.87 N2 O2 P6 Se8

Formula weight 	2146.46

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C 2/c

Unit cell dimensions	a = 20.088(2) Å	= 90°.

b = 15.276(2) Å	= 110.951(10)°.

c = 27.502(3) Å	 = 90°.

Volume	7881.7(17) Å3

Z	4

Density (calculated)	1.809 Mg/m3

Absorption coefficient	5.320 mm-1

F(000)	4262

Crystal size	0.200 x 0.140 x 0.120 mm3

Theta range for data collection	1.586 to 28.327°.

Index ranges	-26<=h<=26, -19<=k<=20, -16<=l<=36

Reflections collected	19157

Independent reflections	9777 [R(int) = 0.0472]

Completeness to theta = 25.000°	99.5 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9777 / 121 / 479

Goodness-of-fit on F2	1.093

Final R indices [I>2sigma(I)]	R1 = 0.0621, wR2 = 0.1366

R indices (all data)	R1 = 0.0933, wR2 = 0.1502

Largest diff. peak and hole	2.081 and -1.159 e.Å-3

Sheldrick, G. M. (2005). CELL_NOW. University of Goettingen, Germany.

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick, G. M. (2007). TWINABS. University of Goettingen, Germany.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565