Crystal Structure Report for J. Kovacs

by Dylan Rogers & Werner Kaminsky

Sample Submitted by Alex Downing

ID – AD3022

X-ray Crystallography Laboratory

University of Washington

25. April 2019

Data Collection  started: 4/23/2019

Documentation finished: 4/25/2019

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A brown shard, measuring 0.12 x 0.07 x 0.04 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 60 seconds per frame for all sets.  The scan width was 1o.   Data collection was 100% complete to 25o  in (.  A total of  2118 merged unique reflections were collected covering the indices, -10<=h<=13, -8<=k<=10, -11<=l<=14, Rint = 0.339. Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be Pc  (No.6).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is acentric non-chiral and twinned 1:1 via inversion. The asymmetric unit shows a slightly distorted molecule (evident when looking along N2-Co1). C12 is slightly tilted off which still enables a hydrogen bond to form with the oxygen O1, but also allows a van der Waals interaction between one methylene hydrogen on C11 and O1. A similar interaction occurs between one methylene hydrogen on C8 and S2, also enabled by the tilt. The S1 O1 distance appears to be relatively short with 1.259(19)Å.

The crystal was very small, thus, the statistical data is weak. However, the structure is edited to enable publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C17 H33 Co F6 N3 O P S2

Formula weight 	563.48

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P c

Unit cell dimensions	a = 11.237(5) Å	= 90°.

b = 9.050(5) Å	= 110.292(5)°.

c = 12.433(5) Å	 = 90°.

Volume	1185.9(10) Å3

Z	2

Density (calculated)	1.578 Mg/m3

Absorption coefficient	1.029 mm-1

F(000)	584

Crystal size	0.12 x 0.07 x 0.04 mm3

Theta range for data collection	1.932 to 25.086°.

Index ranges	-10<=h<=13, -8<=k<=10, -11<=l<=14

Reflections collected	2118

Independent reflections	2118 [R(int) = 0.339]

Completeness to theta = 25.000°	100.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2118 / 183 / 281

Goodness-of-fit on F2	0.858

Final R indices [I>2sigma(I)]	R1 = 0.0916, wR2 = 0.2026

R indices (all data)	R1 = 0.2824, wR2 = 0.2625

Absolute structure parameter	0.5(2)

Largest diff. peak and hole	0.529 and -0.413 e.Å-3

# Endnotes

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565