Crystal Structure Report for K. Goldberg

by Werner Kaminsky

Sample Submitted by Ash Wright

ID – AW4_128

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 2/11/2016

Documentation finished: 2/17/2016

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A yellow prism, measuring 0.08 x 0.05 x 0.02 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per frame for all sets.  The scan width was 1o.   Data collection was 100% complete to 25o  in .  A total of  129547 reflections were collected covering the indices, -16<=h<=16, -27<=k<=27, -20<=l<=21.  9645 reflections were symmetry independent and the Rint = 0.0950 indicated that the data was of moderate quality.  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/n  (No.14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

Solvent analysis discovered delocalized acetic acid and or other solvents, and that contribution to the diffraction pattern was removed with SQUEEZE. In addition, 2.2% of starting material (I2 acetonitrile Ir-complex with the same organic ligand) was found that coincides almost with the main Ir complex. A single large electron density close to O2 belongs to one of the two iodine atoms of the starting material. The acetonitrile and other deviating contributions of the starting complex were below the detection limit, and thus, a chemical disorder model containing the impurity was not attempted.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C82 H70 F6 I2 Ir2 N8 O4

Formula weight 	1983.66

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/n

Unit cell dimensions	a = 12.6014(6) Å	= 90°.

b = 20.7432(12) Å	= 110.150(3)°.

c = 15.8174(7) Å	 = 90°.

Volume	3881.5(3) Å3

Z	2

Density (calculated)	1.697 Mg/m3

Absorption coefficient	4.289 mm-1

F(000)	1928

Crystal size	0.08 x 0.05 x 0.02 mm3

Theta range for data collection	1.69 to 28.34°.

Index ranges	-16<=h<=16, -27<=k<=27, -20<=l<=21

Reflections collected	129547

Independent reflections	9645 [R(int) = 0.0950]

Completeness to theta = 25.00°	100.0 %

Max. and min. transmission	0.9191 and 0.7254

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9645 / 0 / 475

Goodness-of-fit on F2	1.085

Final R indices [I>2sigma(I)]	R1 = 0.0414, wR2 = 0.0822

R indices (all data)	R1 = 0.0649, wR2 = 0.0881

Largest diff. peak and hole	2.304 and -1.615 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

A. Spek, J. Appl. Cryst. (2003), 36, 7-13; P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565