Crystal Structure Report for A. Velian

by Paige Gannon & Werner Kaminsky

Sample Submitted by Ben Mitchell

ID – BMS_622

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 11/2/2021

Documentation finished: 11/16/2021

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A blue needle, measuring 0.58 x 0.05 x 0.03 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.9% complete to 25o  in .  A total of  30057 reflections were collected covering the indices, -15<=h<=15, -18<=k<=18, -27<=l<=27.  15094 reflections were symmetry independent and the slightly elavated Rint = 0.1392 indicated that the data was acceptable.  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P1  (No. 2).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

With the exception of a few DELU – displacement parameter stabilizations of two toluene moieties and ISOR for two other atoms, the structure was freely refined. One DCM was found and the contribution of heavily disordered additional pentane to the diffraction pattern was removed with SQUEEZE

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disordered pentane omitted via SQUEEZE.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C77 H70 Cl2 Co2 N4 O2 P4 Se2

Formula weight 	1553.93

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 12.6942(12) Å	a= 83.006(6)°.

b = 15.1453(14) Å	b= 78.299(5)°.

c = 22.622(2) Å	g = 83.775(6)°.

Volume	4211.5(7) Å3

Z	2

Density (calculated)	1.225 Mg/m3

Absorption coefficient	1.439 mm-1

F(000)	1584

Crystal size	0.580 x 0.050 x 0.030 mm3

Theta range for data collection	1.360 to 25.155°.

Index ranges	-15<=h<=15, -18<=k<=18, -27<=l<=27

Reflections collected	30057

Independent reflections	15094 [R(int) = 0.1392]

Completeness to theta = 25.000°	99.9 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	15094 / 32 / 842

Goodness-of-fit on F2	0.946

Final R indices [I>2sigma(I)]	R1 = 0.0699, wR2 = 0.1553

R indices (all data)	R1 = 0.1654, wR2 = 0.1947

Largest diff. peak and hole	1.222 and -0.860 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

’Sheldrick : A short history of SHELX . Acta Cryst. (2008), A64, 112-122

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565