Crystal Structure Report for D. Gamlin

by Werner Kaminsky

Sample Submitted by Kyle Kluherz

ID – CsPbCl3

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 6/10/2021

Documentation finished: 7/15/2021

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A colorless prism, measuring 0.350 x 0.300 x 0.200 mm3 was mounted inside a closed capillary.  Data was collected at 22oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.1% complete to 25o in .  A total of 1756 merged reflections were collected covering the indices, -10<=h<=10, -14<=k<=14, -10<=l<=10.  969 reflections were symmetry independent and the Rint = 0.0684 indicated that the data was of average quality (0.07).  Indexing and unit cell refinement indicated an orthorhombic lattice (with almost identical a and c axes).  The space group was found to be P n m a (No. 62).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure was solved including a two-fold rotation twin about [-1 0 1].

There is clear evidence of chlorine disorder.

The size of the sample may have been too large, a quarter or even a tenth of volume may prove helpful to avoid absorption correction problems.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	Cl6 Cs2 Pb2

Formula weight 	892.90

Temperature 	296(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P n m a

Unit cell dimensions	a = 7.9014(13) Å	a= 90°.

b = 11.1590(19) Å	b= 90°.

c = 7.8996(13) Å	g = 90°.

Volume	696.5(2) Å3

Z	2

Density (calculated)	4.257 Mg/m3

Absorption coefficient	30.388 mm-1

F(000)	752

Crystal size	0.350 x 0.300 x 0.200 mm3

Theta range for data collection	1.825 to 28.439°.

Index ranges	-10<=h<=10, -14<=k<=14, -10<=l<=10

Reflections collected	1756

Independent reflections	969 [R(int) = 0.0684]

Completeness to theta = 25.000°	99.1 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	969 / 12 / 37

Goodness-of-fit on F2	1.062

Final R indices [I>2sigma(I)]	R1 = 0.0717, wR2 = 0.1713

R indices (all data)	R1 = 0.0933, wR2 = 0.1964

Extinction coefficient	0.0106(13)

Largest diff. peak and hole	5.058 and -6.054 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565