Crystal Structure Report for D. Gamelin

by Paige Gannon & Werner Kaminsky

Sample Submitted by Kyle Kluherz

ID – CsPbCl3_b

X-ray Crystallography Laboratory

University of Washington

30. July 2026

Data Collection  started: 10/4/2021

Documentation finished: 10/29/2021

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A colorless block, measuring 0.15 x 0.10 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 100% complete to 25o  in .  A total of  5208 reflections were collected covering the indices, -9<=h<=9, -13<=k<=13, -9<=l<=9.  740 reflections were symmetry independent, and the Rint = 0.0716 indicated that the data was of average quality (0.07).  Indexing and unit cell refinement indicated a primitive orthorhombic lattice.  The space group was found to be P n m a  (No. 62).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

The data appeared twinned via 90 degrees about [1 0 -1] (CELL_NOW) and after multi-domain integration (SAINT, SADABS within the APEX2 software package by Bruker) the data was merged utilizing twinabs.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The Cs is slightly disordered over three close locations.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the crystal packing. Atoms of the asymmetric unit enumerated.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	Cl12 Cs4 Pb4

Formula weight 	1785.80

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P n m a

Unit cell dimensions	a = 7.9411(6) Å	a= 90°.

b = 11.1914(9) Å	b= 90°.

c = 7.7631(6) Å	g = 90°.

Volume	689.92(9) Å3

Z	1

Density (calculated)	4.298 Mg/m3

Absorption coefficient	30.678 mm-1

F(000)	752

Crystal size	0.150 x 0.100 x 0.050 mm3

Theta range for data collection	3.194 to 26.369°.

Index ranges	-9<=h<=9, -13<=k<=13, -9<=l<=9

Reflections collected	5208

Independent reflections	740 [R(int) = 0.0716]

Completeness to theta = 25.000°	100.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	740 / 19 / 46

Goodness-of-fit on F2	1.140

Final R indices [I>2sigma(I)]	R1 = 0.0260, wR2 = 0.0650

R indices (all data)	R1 = 0.0284, wR2 = 0.0667

Largest diff. peak and hole	1.451 and -1.402 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick, G. M. (2005). CELL_NOW. University of Goettingen, Germany.

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick, G. M. (2007). TWINABS. University of Goettingen, Germany.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565