Crystal Structure Report for B. Cossairt

by Betsy Flowers & W. K.

Sample Submitted by Danielle Henkel

ID – DH2_193

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data backup accessibly through http:

URL: 	http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

An orange piece, measuring 0.10 x 0.07 x 0.02 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 240 seconds per frame for all sets.  The scan width was 1o.   Data collection was 97.7% complete to 25o  in .  A total of  9954 reflections were collected covering the indices, h = -24 to 25, k = -12 to 11,  l = -19 to 17.  2634 reflections were symmetry independent and the Rint = 0.1133 indicated that the crystal was small.  Indexing and unit cell refinement indicated a C-centered monoclinic lattice.  The space group was found to be C 2/c  (No.15).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

A multiple disordered OTF anion accompanied a half Ru complex, completed via symmetry. The anion contribution to the diffraction pattern was removed with SQEEZE as it turned out impossible to catch all OTF orientations with sufficient accuracy.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Anion omitted.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C24 H22 N6 Ru

Formula weight 	495.55

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C 2/c

Unit cell dimensions	a = 22.059(9) Å	= 90°.

b = 10.660(5) Å	= 131.779(16)°.

c = 17.161(5) Å	 = 90°.

Volume	3009(2) Å3

Z	4

Density (calculated)	1.094 Mg/m3

Absorption coefficient	0.538 mm-1

F(000)	1008

Crystal size	0.10 x 0.07 x 0.02 mm3

Theta range for data collection	2.26 to 25.29°.

Index ranges	-24<=h<=25, -12<=k<=11, -19<=l<=17

Reflections collected	9954

Independent reflections	2634 [R(int) = 0.1133]

Completeness to theta = 25.00°	97.7 %

Max. and min. transmission	0.9893 and 0.9482

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2634 / 0 / 142

Goodness-of-fit on F2	0.868

Final R indices [I>2sigma(I)]	R1 = 0.0617, wR2 = 0.1322

R indices (all data)	R1 = 0.1207, wR2 = 0.1482

Largest diff. peak and hole	0.930 and -0.779 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

A. Spek, J. Appl. Cryst. (2003), 36, 7-13; P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565