Crystal Structure Report for J. Kovacs

by Werner Kaminsky & Dylan Rogers

Sample Submitted by Dylan Rogers

ID – DMR1273b

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 10/04/20

Documentation finished: 10/09/20

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A red needle, measuring 0.03 x 0.04 x 0.24 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 90 seconds per degree for all sets.  The scan width was 1o.   Data collection was 99.9% complete to 25o  in .  A total of  8954 merged reflections were collected covering the indices, -16<=h<=16, -15<=k<=15, -18<=l<=18.  4628 reflections were symmetry independent and the Rint = 0.1382 indicated that the data was of worse than average quality (average quality 0.07).  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P 21/c (No.14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C16 H31 F6 Fe N3 O0.80 P S1.20

Formula weight 	517.54

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/c

Unit cell dimensions	a = 13.0383(9) Å	a= 90°.

b = 12.0531(8) Å	b= 101.923(3)°.

c = 14.7542(13) Å	g = 90°.

Volume	2268.6(3) Å3

Z	4

Density (calculated)	1.515 Mg/m3

Absorption coefficient	0.906 mm-1

F(000)	1074

Crystal size	0.24 x 0.04 x 0.03 mm3

Theta range for data collection	1.596 to 26.411°.

Index ranges	-16<=h<=16, -15<=k<=15, -18<=l<=18

Reflections collected	8954

Independent reflections	4628 [R(int) = 0.1382]

Completeness to theta = 25.000°	99.9 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.746 and 0.638

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4628 / 4 / 276

Goodness-of-fit on F2	0.998

Final R indices [I>2sigma(I)]	R1 = 0.0556, wR2 = 0.0900

R indices (all data)	R1 = 0.1833, wR2 = 0.1211

Largest diff. peak and hole	0.487 and -0.478 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565