Crystal Structure Report for

Cherif Ben Nasr

by Werner Kaminsky

ID – DRISS

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 1/23/2017

Documentation finished: 1/25/2017

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A colorless prism, measuring 0.30 x 0.27 x 0.21 mm3 was mounted on a loop with oil.  Data was collected at -143oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 32 mm and exposure time was 35 seconds per degree for all sets.  The scan width was 1.6o.   Data collection was 99.8% complete to 25o  in .  A total of  68023 partial and complete reflections were collected covering the indices, -20<=h<=20, -14<=k<=15, -25<=l<=25.  8056 reflections were symmetry independent and the Rint = 0.0594 indicated that the data was good.  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/n  (No. 14).

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

Some disorder is related to a small amount of water in the structure.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder and water solvent omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C15 H21.13 N2 O4.06 P

Formula weight 	325.43

Temperature 	130(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/n

Unit cell dimensions	a = 15.3175(5) Å	= 90°.

b = 11.7656(5) Å	= 111.483(3)°.

c = 19.4907(6) Å	 = 90°.

Volume	3268.6(2) Å3

Z	8

Density (calculated)	1.323 Mg/m3

Absorption coefficient	0.188 mm-1

F(000)	1381

Crystal size	0.30 x 0.27 x 0.21 mm3

Theta range for data collection	2.06 to 28.30°.

Index ranges	-20<=h<=20, -14<=k<=15, -25<=l<=25

Reflections collected	68023

Independent reflections	8056 [R(int) = 0.0594]

Completeness to theta = 25.00°	99.8 %

Max. and min. transmission	0.9616 and 0.9458

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8056 / 6 / 426

Goodness-of-fit on F2	1.038

Final R indices [I>2sigma(I)]	R1 = 0.0526, wR2 = 0.1298

R indices (all data)	R1 = 0.1001, wR2 = 0.1457

Largest diff. peak and hole	0.397 and -0.441 e.Å-3

Otwinowsky, Z.; Minor, W. In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 1997, 276, 307-326.

(a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565