Crystal Structure Report for A. Velian

by Sebastian Krajewski &Werner Kaminsky

Sample Submitted by Daniel Zhou

ID – Dz431

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 1/23/2023

Documentation finished: 1/26/2023

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A black plate, measuring 0.74 x 0.2 x 0.02 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 45 mm and exposure time was 120 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 96.4% complete to 24.407o in .  A total of 237404 reflections were collected covering the indices, -23<=h<=23, -33<=k<=33, -54<=l<=55.  11672 reflections were symmetry independent and the Rint = 0.1604 indicated that the data was problematic.  Indexing and unit cell refinement indicated a primitive orthorhombic lattice.  The space group was found to be Pcab  (No. 61).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker. Objective outlier removal was achieved with the Bayesian post-processing algorithm from within the SORTAV package.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The sample looked conglomerated, and it is possible that this caused the symmetry to appear pseudo-orthorhombic, but no other symmetry or twin law was found.

The data was weak and of overall rather bad quality. The refinement was requiring global DELU and ISOR restraints in addition to optimizing phenyl groups and relating geometrically similar moieties via SAME cards. The sulfur of the NCS group is showing considerable uncertainty in its location. The contribution of disordered DCM solvent to the diffraction pattern was removed with SQUEEZE. About 700 bad reflections were removed but this is still a small fraction of the total number.

The structure is of mediocre quality but publishable, given some caveats added to a manuscript as outlined. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Solvent omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C115 H102 Co6 Fe3 N7 P6 S Se8

Formula weight 	2952.72

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pcab

Unit cell dimensions	a = 19.402(2) Å	a= 90°.

b = 27.951(4) Å	b= 90°.

c = 46.141(6) Å	g = 90°.

Volume	25022(5) Å3

Z	8

Density (calculated)	1.568 Mg/m3

Absorption coefficient	3.579 mm-1

F(000)	11672

Crystal size	0.74 x 0.2 x 0.02 mm3

Theta range for data collection	1.796 to 24.407°.

Index ranges	-23<=h<=23, -33<=k<=33, -54<=l<=55

Reflections collected	19861

Independent reflections	19861 [R(int) = 0.1604]

Completeness to theta = 24.407°	96.4 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	19861 / 1884 / 1106

Goodness-of-fit on F2	1.004

Final R indices [I>2sigma(I)]	R1 = 0.1921, wR2 = 0.3722

R indices (all data)	R1 = 0.2741, wR2 = 0.4179

Extinction coefficient	0.00030(3)

Largest diff. peak and hole	2.143 and -2.424 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) S. French and K. Wilson (1979). On the Treatment of Negative Intensity Observations. Acta Cryst. A34, 517-525.

(b) Blessing, R. H. (1995). An empirical correction for absorption anisotropy. Acta Cryst. A51 33-38.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,  Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565