Crystal Structure Report for A. Velian

by Sebastian Krajewski &Werner Kaminsky

Sample Submitted by Daniel Zhou

ID – Dz474

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 3/27/2023

Documentation finished: 3/30/2023

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A brown chard, measuring 0.40 x 0.16 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.7% complete to 25o in .  A total of  339061 reflections were collected covering the indices, -25<=h<=25, -39<=k<=39, -30<=l<=30.  32758 reflections were symmetry independent and the Rint = 0.0826 indicated that the data was of average quality.  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/n  (No. 14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

This is a chemically disordered structure, where 21% is the expected cluster-(Fe-NCS)3 species, 79% is the I3 version. The charge of one TBA cation is balanced by a NCS- which appears disordered with one DCM over several locations. Several toluene and phenyl moieties are disordered. To stabilize the displacement parameters and some disordered phenyls, EADP constraints for overlapping atoms and idealization of phenyls were applied in addition to ISOR smoothing of anisotropy for the disordered and some almost disordered moieties. The Fe-N, FeC, and Fe-S distances were linked with SAME and one Fe-NCS was fixed in a AFIX 6 … AFIX 0 loop after setting the N-C, N-S and C-S distance with a strong DFIX. SIMU restraints were applied to I-NCS disordered and NCS DCM disordered moieties.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1a, b show ORTEPs of the two species inside the asymmetric unit.

a)

b)

Figure 1a/b. ORTEP of the structures with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C132.62 H140 Cl2 Co6 Fe3 I2.38 N8.62 P6 S1.62 Se8

Formula weight 	3618.31

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/n

Unit cell dimensions	a = 19.5494(12) Å	a= 90°.

b = 30.0727(19) Å	b= 90.766(3)°.

c = 23.1726(15) Å	g = 90°.

Volume	13622.0(15) Å3

Z	4

Density (calculated)	1.764 Mg/m3

Absorption coefficient	3.884 mm-1

F(000)	7137

Crystal size	0.400 x 0.160 x 0.050 mm3

Theta range for data collection	1.109 to 28.021°.

Index ranges	-25<=h<=25, -39<=k<=39, -30<=l<=30

Reflections collected	339061

Independent reflections	32758 [R(int) = 0.0826]

Completeness to theta = 25.242°	99.7 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	32758 / 698 / 1816

Goodness-of-fit on F2	1.100

Final R indices [I>2sigma(I)]	R1 = 0.0746, wR2 = 0.1432

R indices (all data)	R1 = 0.1185, wR2 = 0.1647

Largest diff. peak and hole	2.034 and -1.555 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,  Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565