Crystal Structure Report for A. Velian

by Sebastian Krajewski & Werner Kaminsky

Sample Submitted by Daniel Zhou

ID – DZ_478

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 4/13/2023

Documentation finished: 4/20/2023

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A bbrown plate, measuring 0.51 x 0.21 x 0.12 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 100% complete to 25o in .  A total of  26546 reflections were collected covering the indices, -37<=h<=37, -37<=k<=37, -70<=l<=70.  181506 reflections were symmetry independent and the Rint = 0.0863 indicated that the data was of average quality (0.07). Indexing and unit cell refinement indicated a body centered tetragonal lattice.  The space group was found to be P 41/a  (No. 88).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The contribution of disordered solvent to the diffraction pattern was removed with SQUEEZE

Similar moieties were related via SAME, and the disordered toluene had the displacment parameters set to be all equal via EADP. Similarly, but less harshly, the diplacements of NCS anion atoms on Fe1A were restraint with SIMU and the distances optimized via DFIX. Examplarily, the ring-methyl distance of toluenes were optimized with DFIX. Soft displacement links were applied to DCM and a few other toluenes and one phenyl.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

a)

b)

Figure 1 a) major, b) minor components. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C116.79 H106.77 Cl4.77 Co6 Fe3 I1.59 N6.41 O0.41 P6 Se8

Formula weight 	3316.35

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	I 41/a

Unit cell dimensions	a = 30.293(2) Å	a= 90°.

b = 30.293(2) Å	b= 90°.

c = 56.600(4) Å	g = 90°.

Volume	51941(8) Å3

Z	16

Density (calculated)	1.696 Mg/m3

Absorption coefficient	3.911 mm-1

F(000)	25970

Crystal size	0.510 x 0.210 x 0.120 mm3

Theta range for data collection	1.192 to 26.372°.

Index ranges	-37<=h<=37, -37<=k<=37, -70<=l<=70

Reflections collected	181506

Independent reflections	26546 [R(int) = 0.0863]

Completeness to theta = 25.242°	100.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	26546 / 1357 / 1463

Goodness-of-fit on F2	1.080

Final R indices [I>2sigma(I)]	R1 = 0.0748, wR2 = 0.1645

R indices (all data)	R1 = 0.1362, wR2 = 0.2006

Largest diff. peak and hole	2.350 and -1.940 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,  Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565