Crystal Structure Report for A. Velian

by Werner Kaminsky

Sample Submitted by Daniel Zhou

ID – DZ759

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 6/18/2024

Documentation finished: 6/24/2024

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A yellow plate, measuring 0.14 x 0.10 x 0.02 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.3% complete to 25o in .  A total of  135871 reflections were collected covering the indices, -16<=h<=16, -20<=k<=20, -30<=l<=30.  20866 reflections were symmetry independent and the Rint = 0.0705 indicated that the data was of  average quality.  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P1  (No. 2).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The contribution of disordered pentane and DCM solvent to the diffraction pattern was removed with SQUEEZE

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Solvent SQUEEZED.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C76 H68 Fe2 N4 O2 P4 Se2

Formula weight 	1462.84

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 12.6482(6) Å	a= 83.508(3)°.

b = 15.3741(7) Å	b= 78.853(3)°.

c = 22.5997(10) Å	g = 82.862(3)°.

Volume	4260.4(3) Å3

Z	2

Density (calculated)	1.140 Mg/m3

Absorption coefficient	1.310 mm-1

F(000)	1496

Crystal size	0.140 x 0.100 x 0.020 mm3

Theta range for data collection	0.922 to 28.375°.

Index ranges	-16<=h<=16, -20<=k<=20, -30<=l<=30

Reflections collected	40475

Independent reflections	20866 [R(int) = 0.0705]

Completeness to theta = 25.242°	99.3 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	20866 / 0 / 815

Goodness-of-fit on F2	0.974

Final R indices [I>2sigma(I)]	R1 = 0.0492, wR2 = 0.1034

R indices (all data)	R1 = 0.1023, wR2 = 0.1177

Largest diff. peak and hole	1.360 and -0.863 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,  Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565