Crystal Structure Report for R Dinda

by Werner Kaminsky

Sample ID – GS_2

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 5/22/2019

Documentation finished: 6/13/2019

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A black prism, measuring 0.45 x 0.24 x 0.12 mm3 was mounted on a loop with oil.  Data was collected at 22oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 30 mm and exposure time was 40 seconds per degree for all sets.  The scan width was 1.9o.   Data collection was 99.8% complete to 25o  in .  A total of  6440 merged partial and complete reflections were collected covering the indices, -15<=h<=15, -10<=k<=11, 0<=l<=19.  3778 reflections were symmetry independent and the Rint = 0.0707 indicated that the data of average quality.  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/n (No.14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure shows rotational disorder in the C2-O2 moiety.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C19 H15 N2 O7 V

Formula weight 	434.27

Temperature 	295(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/n

Unit cell dimensions	a = 12.5199(6) Å	= 90°.

b = 9.3115(5) Å	= 90.20(5)°.

c = 15.6208(11) Å	 = 90°.

Volume	1821.05(18) Å3

Z	4

Density (calculated)	1.584 Mg/m3

Absorption coefficient	0.592 mm-1

F(000)	888

Crystal size	0.450 x 0.240 x 0.120 mm3

Theta range for data collection	2.547 to 26.735°.

Index ranges	-15<=h<=15, -10<=k<=11, 0<=l<=19

Reflections collected	6440

Independent reflections	3778 [R(int) = 0.0707]

Completeness to theta = 25.000°	99.8 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3778 / 53 / 279

Goodness-of-fit on F2	0.902

Final R indices [I>2sigma(I)]	R1 = 0.0671, wR2 = 0.1518

R indices (all data)	R1 = 0.1368, wR2 = 0.1810

Largest diff. peak and hole	0.560 and -0.556 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565