Crystal Structure Report for

Jiun-Haw Chu

by Werner Kaminsky

Sample Submitted by Paul Malinowski

ID – IC832

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 1/26/2021

Documentation finished: 2/10/2021

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A thin metallic black plate, measuring 0.30 x 0.30 x 0.03 mm3 was mounted on a loop with oil.  Data was collected at 296K, 150K, 120K, and 90K on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation (a remount occurred between the 296K and 150K structures).

Crystal-to-detector distance was 40 mm and exposure time was 5 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 80-90% complete to 25o  in .   Indexing and unit cell refinement indicated a R-centered trigonal lattice.  The space group was found to be R3m:H  (No.166).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structures appear similar, except at 120K it seems that the Te is disordered about 1:1 over two positions apart along the c-axis by 0.279 Å. As previously observed, the Ge and one iron are also disordered and a deficiency is observed of about 9% for that iron, which translates to refined sum formulas of the 4 structures from high to low T of GeTe2Fe4.76 / Fe4.803/ Fe4.81/ Fe4.82.

The length of the c-axis also is observed to increase slightly from 150K to 120K before contracting again with lowering of temperature which was ramped down between temperatures at a rate of 300K/hour.

120K packing.

The structures are of high quality and ready for publication. Table 1 summarizes the data collection details.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	Fe14.28 Ge3 Te6

Formula weight 	1780.91

Temperature 	296(2) K

Wavelength 	0.71073 Å

Crystal system 	Trigonal

Space group 	R -3 m :H

Unit cell dimensions	a = 4.0321(4) Å	a= 90°.

b = 4.0321(4) Å	b= 90°.

c = 29.114(3) Å	g = 120°.

Volume	409.92(9) Å3

Z	1

Density (calculated)	7.214 Mg/m3

Absorption coefficient	28.039 mm-1

F(000)	779

Crystal size	0.300 x 0.300 x 0.030 mm3

Theta range for data collection	4.200 to 28.337°.

Index ranges	-5<=h<=5, -5<=k<=5, -37<=l<=37

Reflections collected	646

Independent reflections	154 [R(int) = 0.1353]

Completeness to theta = 25.000°	89.3 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	154 / 0 / 16

Goodness-of-fit on F2	1.258

Final R indices [I>2sigma(I)]	R1 = 0.0698, wR2 = 0.1843

R indices (all data)	R1 = 0.0700, wR2 = 0.1843

Extinction coefficient	0.021(6)

Largest diff. peak and hole	3.266 and -2.173 e.Å-3

Empirical formula 	Fe14.41 Ge3 Te6

Formula weight 	1788.17

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Trigonal

Space group 	R -3 m :H

Unit cell dimensions	a = 4.0226(4) Å	a= 90°.

b = 4.0226(3) Å	b= 90°.

c = 29.052(3) Å	g = 120°.

Volume	407.12(9) Å3

Z	1

Density (calculated)	7.294 Mg/m3

Absorption coefficient	28.343 mm-1

F(000)	783

Crystal size	0.300 x 0.300 x 0.030 mm3

Theta range for data collection	5.897 to 28.576°.

Index ranges	-5<=h<=5, -5<=k<=5, -39<=l<=39

Reflections collected	1207

Independent reflections	142 [R(int) = 0.1914]

Completeness to theta = 25.000°	78.7 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	142 / 0 / 16

Goodness-of-fit on F2	1.176

Final R indices [I>2sigma(I)]	R1 = 0.0560, wR2 = 0.1035

R indices (all data)	R1 = 0.0570, wR2 = 0.1039

Extinction coefficient	0.025(5)

Largest diff. peak and hole	2.163 and -1.871 e.Å-3

Empirical formula 	Fe14.43 Ge3 Te6

Formula weight 	1789.29

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Trigonal

Space group 	R -3 m :H

Unit cell dimensions	a = 4.0234(6) Å	a= 90°.

b = 4.0234(6) Å	b= 90°.

c = 29.080(5) Å	g = 120°.

Volume	407.68(14) Å3

Z	1

Density (calculated)	7.288 Mg/m3

Absorption coefficient	28.322 mm-1

F(000)	783

Crystal size	0.300 x 0.300 x 0.030 mm3

Theta range for data collection	5.896 to 28.235°.

Index ranges	-5<=h<=5, -5<=k<=5, -37<=l<=37

Reflections collected	1153

Independent reflections	139 [R(int) = 0.1983]

Completeness to theta = 25.000°	82.8 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	139 / 6 / 18

Goodness-of-fit on F2	1.178

Final R indices [I>2sigma(I)]	R1 = 0.0594, wR2 = 0.1367

R indices (all data)	R1 = 0.0594, wR2 = 0.1367

Extinction coefficient	0.026(5)

Largest diff. peak and hole	2.690 and -2.263 e.Å-3

Empirical formula 	Fe14.46 Ge3 Te6

Formula weight 	1790.96

Temperature 	90(2) K

Wavelength 	0.71073 Å

Crystal system 	Trigonal

Space group 	R -3 m :H

Unit cell dimensions	a = 4.0203(4) Å	a= 90°.

b = 4.0203(4) Å	b= 90°.

c = 29.020(3) Å	g = 120°.

Volume	406.21(9) Å3

Z	1

Density (calculated)	7.321 Mg/m3

Absorption coefficient	28.450 mm-1

F(000)	784

Crystal size	0.300 x 0.300 x 0.030 mm3

Theta range for data collection	5.900 to 28.357°.

Index ranges	-5<=h<=5, -5<=k<=5, -37<=l<=37

Reflections collected	1150

Independent reflections	138 [R(int) = 0.1936]

Completeness to theta = 25.000°	80.2 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	138 / 0 / 16

Goodness-of-fit on F2	1.148

Final R indices [I>2sigma(I)]	R1 = 0.0552, wR2 = 0.1224

R indices (all data)	R1 = 0.0683, wR2 = 0.1238

Extinction coefficient	0.027(5)

Largest diff. peak and hole	2.696 and -3.243 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.