Crystal Structure Report for A. Velian

by Werner Kaminsky

Sample Submitted by Isabel Friedrichs

ID – IF13

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 8/9/2021

Documentation finished: 8/12/2021

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A brown needle, measuring 0.27 x 0.05 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 90 seconds per frame for all sets.  The scan width was 1o.   Data collection was 97.3% complete to 25o  in .  A total of  34342 unique reflections were collected covering the indices, -15<=h<=14, -28<=k<=28, -42<=l<=42,  Rint = 0.0881. Indexing and unit cell refinement indicated a large triclinic lattice.  The space group was found to be P1  (No. 2).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure exhibits disorder in multiple places, which required one disordered toluene group to be optimized with AFIX 66 loops. A global ISOR was applied to all nitrogen and carbon atoms and a DELU as well including phosphorous and Co15. In addition, some SAME restraints were required on disordered PEt3 and one CNtbutyl, the latter of which required SADI restraints to optimize one CNtbutyl to serve as template for equivalent moieties related with SAME. The displacement parameters of related disordered atoms were linked with EADP cards. A total of 30 bad peaks were excluded from the refinement.

The contribution of disordered solvent (likely toluene) to the diffraction pattern was removed with SQUEEZE

The structure is of moderate quality but possibly publishable with disclaimer. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 30% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C149 H233 Cl2 Co15 N9 P12 Se16

Formula weight 	4740.28

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 12.3418(11) Å	a= 104.621(6)°.

b = 23.914(2) Å	b= 98.145(6)°.

c = 35.439(3) Å	g = 97.380(6)°.

Volume	9870.6(16) Å3

Z	2

Density (calculated)	1.595 Mg/m3

Absorption coefficient	4.341 mm-1

F(000)	4706

Crystal size	0.270 x 0.050 x 0.050 mm3

Theta range for data collection	1.208 to 25.156°.

Index ranges	-15<=h<=14, -28<=k<=28, -42<=l<=42

Reflections collected	34342

Independent reflections	34342 [R(int) = 0.0881]

Completeness to theta = 25.000°	97.3 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	34342 / 2751 / 1799

Goodness-of-fit on F2	0.961

Final R indices [I>2sigma(I)]	R1 = 0.1250, wR2 = 0.2095

R indices (all data)	R1 = 0.4070, wR2 = 0.2730

Largest diff. peak and hole	1.088 and -1.123 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565