Crystal Structure Report for A. Velian

by Dylan Rogers & Werner Kaminsky

Sample Submitted by Jon Kephart

ID – JAK_483

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 9/28/2020

Documentation finished: 10/8/2020

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors.

A black prism, measuring 0.25 x 0.24 x 0.24 mm3 was mounted on a loop with oil.  Data was collected at -183oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 20 seconds per degree for all sets.  The scan width was 1o.  Data collection was 98.9% complete to 25o in .  A total of 50456 merged reflections were collected covering the indices, -76<=h<=68, -18<=k<=18, 0<=l<=39.  25795 reflections were symmetry independent and the low Rint = 0.0345 indicated that the data was excelleny.  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be C 2/c (No. 15).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The contribution of disordered THF, pentane, or ether solvent molecules to the diffraction pattern was removed with SQUEEZE (1911eV in two voids).

Overall, an ISOR for carbons, and nitrogen, to prevent non-positive definite displacement matrices, and a DELU command including carbons, nitrogen and phosphorous were needed relating the displacement parameters along bonds, and 200 bad reflections were removed. A second, very faint, Se-Co cluster was folded into the refined one, which is observed in some notable rest electron density and a slightly elevated R1, possibly because of chemical disorder. Twinning was not detected.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C129 H117 Co6 Cr3 N9 P6 Se8

Formula weight 	3120.39

Temperature 	90(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C 2/c

Unit cell dimensions	a = 64.501(9) Å	a= 90°.

b = 15.308(2) Å	b= 116.246(6)°.

c = 33.309(4) Å	g = 90°.

Volume	29499(7) Å3

Z	8

Density (calculated)	1.405 Mg/m3

Absorption coefficient	2.953 mm-1

F(000)	12400

Crystal size	0.250 x 0.240 x 0.240 mm3

Theta range for data collection	0.704 to 25.027°.

Index ranges	-76<=h<=68, -18<=k<=18, 0<=l<=39

Reflections collected	50456

Independent reflections	25795 [R(int) = 0.0345]

Completeness to theta = 25.000°	98.9 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	25795 / 1182 / 1456

Goodness-of-fit on F2	1.060

Final R indices [I>2sigma(I)]	R1 = 0.0790, wR2 = 0.1904

R indices (all data)	R1 = 0.0943, wR2 = 0.1984

Largest diff. peak and hole	5.035 and -1.265 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565