Crystal Structure Report for

Sei-Hum Jang

by Werner Kaminsky

Sample ID – JANGNMA01

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 6/16/2020

Documentation finished: 6/19/2020

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A colorless plate, measuring 0.07 x 0.05 x 0.03 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 34 mm and exposure time was 150 seconds per degree for all sets.  The scan width was 1o.   Data collection was 99.9% complete to 25o  in .  A total of   88381 full and partial reflections were collected covering the indices, -15<=h<=14, -15<=k<=14, -34<=l<=33.  A total of 12757 merged and 7626 symmetry independent reflections with Rint = 0.0844 were collected.  Indexing and unit cell refinement indicated a C-centered monoclinic lattice.  The space group was found to be Cc  (No.9).

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The crystal showed a small amount (ca. 5%) of merohedral twinning via twin matrix (0 1 0, 1 0 0, -0.5 -0.5 -1). Furthermore, the structure is non-centrosymmetric – non-chiral, with flack enantiopole parameter -0.010(9), thus showing no acentric twinning.

All organic molecules in the asymmetric unit are disordered ratios close to 1:1 (this is not a sign of crystal quality or any possible decomposition).

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C28 H40 I8 N4 Pb2

Formula weight 	1862.22

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C c

Unit cell dimensions	a = 12.6777(6) Å	a= 90°.

b = 12.6801(6) Å	b= 102.791(2)°.

c = 28.6177(16) Å	g = 90°.

Volume	4486.3(4) Å3

Z	4

Density (calculated)	2.757 Mg/m3

Absorption coefficient	13.023 mm-1

F(000)	3296

Crystal size	0.070 x 0.050 x 0.030 mm3

Theta range for data collection	0.730 to 25.186°.

Index ranges	-15<=h<=14, -15<=k<=14, -34<=l<=33

Reflections collected	12757

Independent reflections	7626 [R(int) = 0.0844]

Completeness to theta = 25.000°	99.9 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7626 / 1022 / 488

Goodness-of-fit on F2	1.016

Final R indices [I>2sigma(I)]	R1 = 0.0561, wR2 = 0.1249

R indices (all data)	R1 = 0.0805, wR2 = 0.1362

Absolute structure parameter	-0.010(9)

Largest diff. peak and hole	3.289 and -2.738 e.Å-3

Otwinowsky, Z.; Minor, W. In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 1997, 276, 307-326.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565