Crystal Structure Report for D. M. Heinekey

by Maike Blakely &Werner Kaminsky

Sample Submitted by Jonathan Goldberg

ID – JMG_C_184

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 6/5/2017

Documentation finished: 6/9/2017

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A yellow prism, measuring 0.37 x 0.05 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 120 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 100% complete to 25o  in .  A total of  37939 reflections were collected covering the indices, -76<=h<=77, -10<=k<=10, -28<=l<=28.  5924 reflections were symmetry independent and the elevated Rint = 0.0543 shows the data was better than average (Rint = 0.07).  Indexing and unit cell refinement indicated a face-centered orthorhombic lattice.  The space group was found to be F dd2  (No. 43). The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

Two bimetallic Ir species co-crystallized, the major component (70.325%) is four coordinate species with a CO ligand, and the minor component (29.675%) is a six coordinate Ir-hydride with a CO and chloride bound. The tert-butyl groups shift due to the presence of the hydride and chloride ion, thus were adjusted using a disordered model. Since X-ray diffraction occurs in response to the average over the whole sample volume, it is also possible that next to the shown ORTEPs of pure dimeric molecules in figure 1 and 2, which contain a crystallographic symmetry element relating their two equivalent parts, a mixed species could be present as well despite local symmetry violation. A disordered toluene molecule is also part of the structure. The structure is of high quality and ready for publication. Table 1 summarizes the data collection details.

Figure 1. ORTEP of the major component structure with thermal ellipsoids at the 50% probability level. Disordered solvent and hydrogen omitted for clarity.

Figure 2. ORTEP of the minor component structure with thermal ellipsoids at the 50% probability level. Disordered solvent and hydrogen omitted for clarity except the hydride, H31.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C53 H84.60 Cl0.60 Ir2 O6 P4

Formula weight 	1347.22

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	F dd2

Unit cell dimensions	a = 62.362(8) Å	= 90°.

b = 8.1450(11) Å	= 90°.

c = 22.807(4) Å	 = 90°.

Volume	11585(3) Å3

Z	8

Density (calculated)	1.545 Mg/m3

Absorption coefficient	4.772 mm-1

F(000)	5398

Crystal size	0.37 x 0.05 x 0.05 mm3

Theta range for data collection	1.306 to 26.378°.

Index ranges	-76<=h<=76, -10<=k<=10, -28<=l<=28

Reflections collected	37939

Independent reflections	5924 [R(int) = 0.0543]

Completeness to theta = 25.00°	100.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5924 / 97/ 335

Goodness-of-fit on F2	1.033

Final R indices [I>2sigma(I)]	R1 = 0.0273, wR2 = 0.0555

R indices (all data)	R1 = 0.0316, wR2 = 0.0567

Largest diff. peak and hole	1.356  and -1.455 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565