Crystal Structure Report for K. Goldberg

by Werner Kaminsky and Dylan Rogers

Sample Submitted by Karena Smoll

ID – KAS-V-48

X-ray Crystallography Laboratory

University of Washington

24. April 2018

Data Collection  started: 4/20/2018

Documentation finished: 4/24/2018

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A black piece, measuring 0.18 x 0.12 0.04 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 100% complete to 25o  in (.  A total of  227802 reflections were collected covering the indices, -19<=h<=19, -22<=k<=22, -21<=l<=21.  9836 reflections were symmetry independent and the Rint = 0.0538 indicated that the data was of better than average quality (0.07).  Indexing and unit cell refinement indicated a monoclinic lattice.  The space group was found to be P21/n  (No.14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure consists of three compounds differing in anion only, two of which are balanced by an acetate anion and one of which is balanced by a chloride anion.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.    Top: C42 H35 Cl1 Ir2 N10 O2. Bottom:  C44 H38 Ir2 N10 O4

Table 1: Crystallographic data for the structures provided.

Table 1.  Crystal data and structure refinement for kas_v_48_0m.

Empirical formula 	C43.32 H36.98 Cl0.34 Ir2 N10 O3.32

Formula weight 	1147.24

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/n

Unit cell dimensions	a = 14.5814(14) Å	= 90°.

b = 16.9229(15) Å	= 91.741(5)°.

c = 15.8899(15) Å	 = 90°.

Volume	3919.2(6) Å3

Z	4

Density (calculated)	1.944 Mg/m3

Absorption coefficient	6.864 mm-1

F(000)	2213

Crystal size	0.180 x 0.120 x 0.040 mm3

Theta range for data collection	1.758 to 28.428°.

Index ranges	-19<=h<=19, -22<=k<=22, -21<=l<=21

Reflections collected	227802

Independent reflections	9836 [R(int) = 0.0538]

Completeness to theta = 25.000°	99.9 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9836 / 25 / 570

Goodness-of-fit on F2	1.092

Final R indices [I>2sigma(I)]	R1 = 0.0236, wR2 = 0.0518

R indices (all data)	R1 = 0.0334, wR2 = 0.0564

Largest diff. peak and hole	1.666 and -0.767 e.Å-3

# Endnotes

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565