Crystal Structure Report for S Jenekhe

by Werner Kaminsky

Sample Submitted by Xiaomei Ding

ID – LTX_hd

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 4/12/2021

Documentation finished: 5/10/2021

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A black prism, measuring 0.30 x 0.25 x 0.10 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 150 seconds per frame for all sets.  The scan width was 0.75o.   Data collection was 100% complete to 20.816o  in .  A total of  13825 reflections were collected covering the indices, -35<=h<=30, 0<=k<=66, 0<=l<=22, Rint = 0.1893 indicated that the data was very weak.  Indexing and unit cell refinement indicated a C-centered monoclinic lattice.  The space group was found to be Cc  (No. 9).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

The contribution of disordered solvent to the diffraction pattern was removed with SQUEEZE

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The side chains appear to be close and disordered, which was not resolvable due to the weakness of the data.

The structure is of such limited quality that publication is only possible with a reclaimer that the data provided ocan only be used to confirm connectivity.

Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 5% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C134 H160 N6 S4

Formula weight 	1982.91

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C c

Unit cell dimensions	a = 29.872(4) Å	a= 90°.

b = 55.816(9) Å	b= 122.556(7)°.

c = 18.769(2) Å	g = 90°.

Volume	26377(7) Å3

Z	8

Density (calculated)	0.999 Mg/m3

Absorption coefficient	0.118 mm-1

F(000)	8560

Crystal size	0.300 x 0.150 x 0.100 mm3

Theta range for data collection	1.361 to 20.816°.

Index ranges	-35<=h<=30, 0<=k<=66, 0<=l<=22

Reflections collected	13825

Independent reflections	13825 [R(int) = 0.1893]

Completeness to theta = 20.816°	100.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	13825 / 6861 / 2449

Goodness-of-fit on F2	1.082

Final R indices [I>2sigma(I)]	R1 = 0.2014, wR2 = 0.4160

R indices (all data)	R1 = 0.4699, wR2 = 0.5770

Absolute structure parameter	0.8(6)

Largest diff. peak and hole	0.592 and -0.446 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565