Crystal Structure Report for J. Kovacs

by Werner Kaminsky

Sample Submitted by Maks Dedushko

ID – MD012120

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 1/21/2020

Documentation finished: 1/22/2020

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A black octahedron, measuring 0.17 x 0.15 x 0.14 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.9% complete to 25o  in .  A total of  41759 reflections were collected covering the indices, -19<=h<=19, -29<=k<=29, -39<=l<=39.  5954 reflections were symmetry independent and the Rint = 0.0574 indicated that the data was good.  Indexing and unit cell refinement indicated a body-centered orthorhombic lattice.  The space group was found to be I c a b  (No. 73).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The contribution of disordered solvent to the diffraction pattern, located inside several infinite channels in different directions, was removed with SQUEEZE. In addition does the structure exhibit some disorder.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C22 H50 F12 Fe2 N8 O P2 S2

Formula weight 	908.46

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Icab

Unit cell dimensions	a = 14.6679(9) Å	a= 90°.

b = 22.026(2) Å	b= 90°.

c = 29.4207(18) Å	g = 90°.

Volume	9505.0(12) Å3

Z	8

Density (calculated)	1.270 Mg/m3

Absorption coefficient	0.838 mm-1

F(000)	3744

Crystal size	0.170 x 0.150 x 0.140 mm3

Theta range for data collection	1.849 to 28.379°.

Index ranges	-19<=h<=19, -29<=k<=29, -39<=l<=39

Reflections collected	41759

Independent reflections	5954 [R(int) = 0.0574]

Completeness to theta = 25.000°	99.9 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5954 / 0 / 245

Goodness-of-fit on F2	1.044

Final R indices [I>2sigma(I)]	R1 = 0.0466, wR2 = 0.1274

R indices (all data)	R1 = 0.0687, wR2 = 0.1424

Largest diff. peak and hole	1.154 and -0.774 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565