Crystal Structure Report for K Goldberg

by Werner Kaminsky

Sample Submitted by M Johnson

ID – MJ253

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 4/14/2015

Documentation finished: 4/22/2015

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A yellow piece, measuring 0.16 x 0.14 x 0.10 mm3 was mounted on a loop with oil.  Data was collected at -183oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 92.4 % complete to 25o  in .  A total of  104506 reflections were collected covering the indices, h = -23 to 23, k = -23to 23,  l = -21 to 21.  3120 reflections were symmetry independent and the Rint = 0.0689 indicated that the data was of average quality 0.07.  Indexing and unit cell refinement indicated a body centered tetragonal lattice.  The space group was found to be I 41 m d (No.109).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The crystals tend to grow as merohedral penetration twins, with invisible boundaries. Thus, it was difficult to find an untwinned sample. Void analysis discovered delocalized solvent (18 electrons per 72 Å3 in 4 voids of the unit cell), presumably water, and that contribution to the diffraction pattern was removed with SQEEZE. The molecule exhibits mirror symmetry through the Rh and phenyl. Elongated displacement ellipsoids especially of the methoxy group indicate some librative motion, indistinguishable from positional disorder. The chloroform hydrogen bonds to Cl2, the disordered  methyl hydrogens on C15 ‘face’ the chlorides of the chloroform, with distances narrowly outside hydrogen bonding.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C21 H21 Cl5 N3 O Rh

Formula weight 	611.57

Temperature 	296(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	I 41 m d

Unit cell dimensions	a = 17.8815(8) Å	= 90°.

b = 17.8815(8) Å	= 90°.

c = 16.0054(11) Å	 = 90°.

Volume	5117.7(5) Å3

Z	8

Density (calculated)	1.587 Mg/m3

Absorption coefficient	1.208 mm-1

F(000)	2448

Crystal size	0.16 x 0.14 x 0.10 mm3

Theta range for data collection	1.71 to 28.37°.

Index ranges	-23<=h<=23, -23<=k<=23, -21<=l<=21

Reflections collected	104506

Independent reflections	3120 [R(int) = 0.0689]

Completeness to theta = 25.00°	92.4 %

Max. and min. transmission	0.8888 and 0.8302

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3120 / 1 / 163

Goodness-of-fit on F2	1.062

Final R indices [I>2sigma(I)]	R1 = 0.0526, wR2 = 0.1325

R indices (all data)	R1 = 0.0544, wR2 = 0.1342

Absolute structure parameter	-0.06(6)

Largest diff. peak and hole	2.164 and -1.610 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

A. Spek, J. Appl. Cryst. (2003), 36, 7-13; P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565