Crystal Structure Report for B. Cossairt

by Sarah Flowers and Werner Kaminsky

Sample Submitted by Michael Norris

ID – MN2_020

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 6 June 2015

Documentation finished: 24 July 2015

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

An orange prism, measuring 0.53 x 0.06 x 0.01 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 240 seconds per frame for all sets.  The scan width was 1o.   Data collection was 96.1% complete to 25o  in .  A total of  55294 reflections were collected covering the indices, h = -29 to 30, k = -13 to 13,  l = -29 to 32.  12455 reflections were symmetry independent and the Rint = 0.0732 indicated that the data was of average quality.  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/n  (No.14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

Solvent analysis discovered infinite channels inside the structure filled with DCM/Acetone and possibly nBu4NCl, the contributions of which to the diffraction pattern was removed with SQUEEZE

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C68 H62 Cl4 N12 P2 Ru2

Formula weight 	1453.18

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/n

Unit cell dimensions	a = 25.6189(16) Å	= 90°.

b = 11.1698(6) Å	= 110.045(3)°.

c = 26.1500(16) Å	 = 90°.

Volume	7029.7(7) Å3

Z	4

Density (calculated)	1.373 Mg/m3

Absorption coefficient	0.675 mm-1

F(000)	2960

Crystal size	0.53 x 0.06 x 0.01 mm3

Theta range for data collection	1.69 to 25.86°.

Index ranges	-29<=h<=30, -13<=k<=13, -29<=l<=32

Reflections collected	55294

Independent reflections	12455 [R(int) = 0.0732]

Completeness to theta = 25.00°	96.1 %

Max. and min. transmission	0.9933 and 0.7161

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	12455 / 42 / 793

Goodness-of-fit on F2	1.037

Final R indices [I>2sigma(I)]	R1 = 0.0658, wR2 = 0.1329

R indices (all data)	R1 = 0.1040, wR2 = 0.1439

Largest diff. peak and hole	1.220 and -1.560 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

A. Spek, J. Appl. Cryst. (2003), 36, 7-13; P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565