Crystal Structure Report for K.SARAVANA MANI

by Werner Kaminsky &

Sebastian Krajewski

Sample ID – Mani_RDE

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 4/7/2025

Documentation finished: 4/8/2025

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A colorless prism, measuring 0.46 x 0.17 x 0.13 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 3 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.9% complete to 25o in .  A total of  210667 reflections were collected covering the indices, -21<=h<=21, -26<=k<=26, -23<=l<=23.  6890 reflections were symmetry independent and the Rint = 0.0449 indicated that the data was of good quality.  Indexing and unit cell refinement indicated a C-centered monoclinic lattice.  The space group was found to be C 2/c  (No. 15).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure contains heavily disordered DMA solvent which takes part in several hydrogen bond interactions with the organic compound.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity. Some hydrogen  bonds were indicated by dashed lines.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C85 H95 N13 O9

Formula weight 	1442.73

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C 2/c

Unit cell dimensions	a = 18.1592(14) Å	a= 90°.

b = 21.7247(16) Å	b= 103.905(4)°.

c = 19.6737(14) Å	g = 90°.

Volume	7533.9(10) Å3

Z	4

Density (calculated)	1.272 Mg/m3

Absorption coefficient	0.084 mm-1

F(000)	3072

Crystal size	0.460 x 0.170 x 0.130 mm3

Theta range for data collection	1.488 to 25.348°.

Index ranges	-21<=h<=21, -26<=k<=26, -23<=l<=23

Reflections collected	210667

Independent reflections	6890 [R(int) = 0.0449]

Completeness to theta = 25.242°	99.9 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6890 / 525 / 596

Goodness-of-fit on F2	1.031

Final R indices [I>2sigma(I)]	R1 = 0.0505, wR2 = 0.1371

R indices (all data)	R1 = 0.0613, wR2 = 0.1490

Largest diff. peak and hole	0.618 and -0.347 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,  Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565