Crystal Structure Report for A. Vignesh

by Werner Kaminsky

Sample

ID – PdBNBH

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 4/26/2016

Documentation finished: 5/3/2016

Data backup accessibly through http:

URL: 	http://cad4.cpac.washington.edu/structures

Username: 	xray-user

Password: 	hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A yellowish prism, measuring 0.40 x 0.19 x 0.14 mm3 was mounted on a loop with oil.  Data was collected at 21oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 30 mm and exposure time was 120 seconds per degree for all sets.  The scan width was 1o.   Data collection was 99.4% complete to 25o  in .  A total of  13619 partial and complete reflections were collected covering the indices, -13<=h<=13, -13<=k<=12, -22<=l<=22.  8249 reflections were symmetry independent and the Rint = 0.0778 indicated that the data was of average quality.  Indexing and unit cell refinement indicated a triclinic P lattice.  The space group was found to be P1  (No.2).

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C39 H31 Cl N3 O4 P Pd

Formula weight 	778.49

Temperature 	294(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 10.4594(8) Å	= 81.230(2)°.

b = 10.3830(7) Å	= 79.326(2)°.

c = 17.1217(12) Å	 = 74.501(4)°.

Volume	1750.4(2) Å3

Z	2

Density (calculated)	1.477 Mg/m3

Absorption coefficient	0.698 mm-1

F(000)	792

Crystal size	0.40 x 0.19 x 0.14 mm3

Theta range for data collection	2.04 to 28.30°.

Index ranges	-13<=h<=13, -13<=k<=12, -22<=l<=22

Reflections collected	13619

Independent reflections	8249 [R(int) = 0.0778]

Completeness to theta = 25.00°	99.4 %

Max. and min. transmission	0.9087 and 0.7678

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8249 / 0 / 443

Goodness-of-fit on F2	1.018

Final R indices [I>2sigma(I)]	R1 = 0.0549, wR2 = 0.1028

R indices (all data)	R1 = 0.1529, wR2 = 0.1387

Extinction coefficient	0.0025(7)

Largest diff. peak and hole	0.432 and -0.996 e.Å-3

Otwinowsky, Z.; Minor, W. In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 1997, 276, 307-326.

(a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565