Crystal Structure Report for

Daniel Gamelin

by Werner Kaminsky and

Sebastian Krajewski

Sample Submitted by Rachel Tenney

ID – RT_2_18

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 2/22/2024

Documentation finished: 2/23/2024

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A green block, measuring 0.12 x 0.10 x 0.03 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 8 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 92.7% complete to 25o in .  A total of  11608 reflections were collected covering the indices, -8<=h<=7, -8<=k<=8, -26<=l<=26.  324 reflections were symmetry independent and the Rint = 0.0309 indicated that the data was brilliant.  Indexing and unit cell refinement indicated a body-centered tetragonal lattice.  The space group was found to be I 4/m m m  (No. 139).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

One chlorine atom appeared to be disordered.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the expanded structure with thermal ellipsoids at the 50% probability level. Cr1, Cl1, and Cs1 are aligned on the c-axis, Cl2 (disordered with Cl3) is aligned with the a-axis.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	Cl4 Cr Cs2

Formula weight 	459.62

Temperature 	296(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	I 4/m m m

Unit cell dimensions	a = 5.1817(3) Å	a= 90°.

b = 5.1817(3) Å	b= 90°.

c = 16.4029(8) Å	g = 90°.

Volume	440.42(6) Å3

Z	2

Density (calculated)	3.466 Mg/m3

Absorption coefficient	10.559 mm-1

F(000)	404

Crystal size	0.120 x 0.100 x 0.030 mm3

Theta range for data collection	2.483 to 34.983°.

Index ranges	-8<=h<=7, -8<=k<=8, -26<=l<=26

Reflections collected	11608

Independent reflections	324 [R(int) = 0.0309]

Completeness to theta = 25.242°	92.7 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	324 / 0 / 15

Goodness-of-fit on F2	1.304

Final R indices [I>2sigma(I)]	R1 = 0.0105, wR2 = 0.0251

R indices (all data)	R1 = 0.0105, wR2 = 0.0251

Extinction coefficient	0.0112(11)

Largest diff. peak and hole	1.294 and -0.618 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,  Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565