Crystal Structure Report for S. Adhikari

by Werner Kaminsky

Sample

ID – SA_SO_373_RT

X-ray Crystallography Laboratory

University of Washington

30. July 2026

Data Collection  started: 11/16/2023

Documentation finished: 11/18/2023

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A pale green block, measuring 0.4 x 0.30 x 0.2 mm3 was mounted on a loop with oil.  Data was collected at 22oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 50 seconds per degree for all sets.  The scan width was 1.5o.   Data collection was 99.2% complete to 25o in .  A total of 195054 reflections were collected covering the indices, -15<=h<=15, -17<=k<=17, -19<=l<=18.  9254 symmetry independent reflections with Rint = 0.0826 were collected.  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P1  (No.2).

The data was integrated and scaled using hkl-SCALEPACK.

Solution by direct methods (SHELXS, SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The unit cell contains several molecules:

C18 H28 F4 N10 Ni,

C18 H26 F4 N10 Ni  (charge 2-)

2(C9 H15 N5) (charge 2+)

2(C9 H14 N5),

4(H Cl)

7(H2 O),

Where the Ni-complexes are completed by inversion through the Ni.

One Water is distributed over 4 locations.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C72 H130 Cl4 F8 N40 Ni2 O7

Formula weight 	2079.37

Temperature 	295(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 12.8235(6) Å	a= 62.530(3)°.

b = 14.7832(7) Å	b= 83.716(3)°.

c = 16.1679(9) Å	g = 72.908(3)°.

Volume	2598.1(2) Å3

Z	1

Density (calculated)	1.329 Mg/m3

Absorption coefficient	0.546 mm-1

F(000)	1094

Crystal size	0.400 x 0.300 x 0.200 mm3

Theta range for data collection	1.420 to 25.154°.

Index ranges	-15<=h<=15, -17<=k<=17, -19<=l<=18

Reflections collected	17716

Independent reflections	9254 [R(int) = 0.0826]

Completeness to theta = 25.154°	99.2 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9254 / 572 / 623

Goodness-of-fit on F2	1.005

Final R indices [I>2sigma(I)]	R1 = 0.0719, wR2 = 0.1478

R indices (all data)	R1 = 0.1331, wR2 = 0.1722

Largest diff. peak and hole	0.677 and -0.543 e.Å-3

Otwinowsky, Z.; Minor, W. (1997) In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 276, 307-326.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. (1995), 51, 416.

Farrugia, L. (1997) J. Appl. Cryst. 30, 565