Crystal Structure Report for

Suman Adhikari

by Werner Kaminsky

ID – SA_SO_380_RT

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started: 3/28/2023

Documentation finished: 4/2/2024

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A colorless prism, measuring 0.12 x 0.08 x 0.06 mm3 was mounted on a loop with oil.  Data was collected at 22oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 150 seconds per degree for all sets.  The scan width was 1o.   Data collection was 100% complete to 25o  in .  A total of  83397 partial and complete reflections were collected covering the indices, -9<=h<=9, -11<=k<=11, -26<=l<=26.  A total of 5955 merged and 3094 symmetry independent reflections with Rint = 0.0225 were collected.  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/n (No. 14).

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C10 H18 Cd N6 S2

Formula weight 	398.82

Temperature 	295(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/n

Unit cell dimensions	a = 7.76130(10) Å	a= 90°.

b = 9.0927(2) Å	b= 94.4720(10)°.

c = 21.5321(5) Å	g = 90°.

Volume	1514.92(5) Å3

Z	4

Density (calculated)	1.749 Mg/m3

Absorption coefficient	1.713 mm-1

F(000)	800

Crystal size	0.120 x 0.080 x 0.060 mm3

Theta range for data collection	1.897 to 26.371°.

Index ranges	-9<=h<=9, -11<=k<=11, -26<=l<=26

Reflections collected	5955

Independent reflections	3094 [R(int) = 0.0225]

Completeness to theta = 25.242°	100.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3094 / 0 / 184

Goodness-of-fit on F2	1.082

Final R indices [I>2sigma(I)]	R1 = 0.0350, wR2 = 0.0849

R indices (all data)	R1 = 0.0464, wR2 = 0.0891

Largest diff. peak and hole	1.851 and -1.375 e.Å-3

Otwinowsky, Z.; Minor, W. In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 1997, 276, 307-326.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565