Crystal Structure Report for S. Adhikari

by Werner Kaminsky

ID – SA_SO_467

X-ray Crystallography Laboratory

University of Washington

29. July 2026

Data Collection  started: 8/19/2024

Documentation finished: 8/29/204

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A colorless needle, measuring 0.26 x 0.10 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 60 seconds per degree for all sets.  The scan width was 2o.   Data collection was 100% complete to 25o  in .  A total of 79627 full and partial, 5845 merged reflections were collected covering the indices, -9<=h<=10, -17<=k<=17, -16<=l<=16.  2998 symmetry independent reflections with Rint = 0.0434 were collected.  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/c (No. 14).

The data was integrated and scaled using hkl-SCALEPACK.

Solution by direct methods (SHELXS, SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C14 H13 N5 O5

Formula weight 	331.29

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/c

Unit cell dimensions	a = 8.0326(4) Å	a= 90°.

b = 13.8160(8) Å	b= 95.117(2)°.

c = 13.3439(11) Å	g = 90°.

Volume	1474.98(17) Å3

Z	4

Density (calculated)	1.492 Mg/m3

Absorption coefficient	0.117 mm-1

F(000)	688

Crystal size	0.260 x 0.100 x 0.050 mm3

Theta range for data collection	2.126 to 26.396°.

Index ranges	-9<=h<=10, -17<=k<=17, -16<=l<=16

Reflections collected	5845

Independent reflections	2998 [R(int) = 0.0434]

Completeness to theta = 25.242°	100.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2998 / 0 / 228

Goodness-of-fit on F2	1.033

Final R indices [I>2sigma(I)]	R1 = 0.0580, wR2 = 0.1441

R indices (all data)	R1 = 0.1129, wR2 = 0.1787

Largest diff. peak and hole	0.282 and -0.279 e.Å-3

Otwinowsky, Z.; Minor, W. (1997) In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 276, 307-326.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. (1995), 51, 416.

Farrugia, L. (1997) J. Appl. Cryst. 30, 565