Crystal Structure Report for R. Dinda

by Werner Kaminsky

Sample Submitted by R. Dinda

ID – SP_2

X-ray Crystallography Laboratory

University of Washington

30. July 2026

Data backup accessibly through http:

URL: 	http://cad4.cpac.washington.edu/structures

Username: 	xray-user

Password: 	hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A red prism, measuring 0.10 x 0.07 x 0.06 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per degree for all sets.  The scan width was 0.5o.   Data collection was 99.9% complete to 25o  in .  A total of  92971 reflections were collected covering the indices, h = -10 to 10, k = -25 to 25,  l = -23 to 23.  6157 reflections were symmetry independent and the Rint = 0.0505 indicated that the data was better than average quality (0.07).  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/c  (No.14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

Nitrogen N6 double bonds to the molybdenum center of the complex at a distance of 1.8557(17) Å, whereas the adjacent N3 single bonds at a bond distance of 2.1372(17) Å. All oxygen atoms single bond to Mo1 with the exception of O4.

Hydrogen bonding is observed, see Table 1.

The structure is of high quality and ready for publication. Table 2 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1.  Hydrogen bonds for sp_2_0ma [Å and °].

____________________________________________________________________________

D-H...A	d(D-H)	d(H...A)	d(D...A)	<(DHA)

____________________________________________________________________________

N(1)-H(1M)...O(2)#1	0.82(3)	2.35(3)	3.149(3)	166(2)

N(1)-H(1N)...N(2)	0.82(3)	2.10(3)	2.742(3)	135(2)

____________________________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x,-y+1/2,z+1/2

Table 2: Crystallographic data for the structures provided.

Empirical formula 	C27 H26 Mo N6 O4

Formula weight 	594.48

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/c

Unit cell dimensions	a = 7.6711(10) Å	= 90°.

b = 18.760(2) Å	= 97.836(6)°.

c = 17.352(2) Å	 = 90°.

Volume	2473.7(5) Å3

Z	4

Density (calculated)	1.596 Mg/m3

Absorption coefficient	0.578 mm-1

F(000)	1216

Crystal size	0.10 x 0.07 x 0.06 mm3

Theta range for data collection	2.17 to 28.39°.

Index ranges	-10<=h<=10, -25<=k<=25, -23<=l<=23

Reflections collected	92971

Independent reflections	6157 [R(int) = 0.0505]

Completeness to theta = 25.00°	99.9 %

Max. and min. transmission	0.9661 and 0.9445

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6157 / 0 / 355

Goodness-of-fit on F2	1.082

Final R indices [I>2sigma(I)]	R1 = 0.0300, wR2 = 0.0660

R indices (all data)	R1 = 0.0407, wR2 = 0.0704

Largest diff. peak and hole	1.055 and -0.813 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS

(version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.

Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565