Crystal Structure Report for K Goldberg

by Werner Kaminsky

Sample Submitted by Timothy Brewster

ID – TB_2_141

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 1/12/2015

Documentation finished: 1/23/2015

Data backup accessibly through http:

URL: 	http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

An orange prism, measuring 0.45 x 0.40 x 0.37  mm3 was mounted on a loop with oil.  Data was collected at 21oC on a Nonius Kappa CCD FR590 single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 30 mm and exposure time was 60 seconds per degree for all sets.  The scan width was 1o.   Data collection was 99.8% complete 25o  in .  A total of  23089 merged reflections were collected covering the indices, h = -15 to 16, k = -18 to 19,  l = -21 to 20.  13944 reflections were symmetry independent and the Rint = 0.0372 indicated that the data was brilliant.  Indexing and unit cell refinement indicated a triclinic P lattice.  The space group was found to be P1  (No.2).

The data was integrated and scaled using hkl-SCALEPACK. This program applies a multiplicative correction factor (S) to the observed intensities (I) and has the following form:

S is calculated from the scale and the B factor determined for each frame and is then applied to I to give the corrected intensity (Icorr).

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The data were taken at 294K because upon cooling the material undergoes a structural phase transition. Delayed recovery to its original clear room-temperature structure is observed after removal of sample from the cold stream, where opaqueness vanishes within a few minutes. Likely, this is a order-disorder case of reversible structural phasetransition where disordered TP* and several CF3 moieties on BArF order into at least two orientations in a different unit cell and symmetry, details pending.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C54 H39 B Cl F24 N2 O2 Rh

Formula weight 	1353.04

Temperature 	294(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 12.6380(2) Å	= 80.517(1)°.

b = 14.6131(2) Å	= 78.680(1)°.

c = 16.1084(3) Å	 = 83.540(1)°.

Volume	2867.27(8) Å3

Z	2

Density (calculated)	1.567 Mg/m3

Absorption coefficient	0.465 mm-1

F(000)	1352

Crystal size	0.45 x 0.40 x 0.37 mm3

Theta range for data collection	2.26 to 28.33°.

Index ranges	-15<=h<=16, -18<=k<=19, -21<=l<=20

Reflections collected	23089

Independent reflections	13944 [R(int) = 0.0372]

Completeness to theta = 25.00°	99.8 %

Max. and min. transmission	0.8469 and 0.8182

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	13944 / 140 / 978

Goodness-of-fit on F2	1.037

Final R indices [I>2sigma(I)]	R1 = 0.0527, wR2 = 0.1351

R indices (all data)	R1 = 0.0961, wR2 = 0.1599

Largest diff. peak and hole	0.545 and -0.845 e.Å-3

Otwinowsky, Z.; Minor, W. In: Methods in Enzymology; Carter, C. W., Jr., Sweet, R. M., Eds.; Academic Press: New York, 1997, 276, 307-326.

(a) Altomare, A.; Burla, C.; Camalli M.; Cascarano L.; Giacovazzo C.; Guagliardi A.;   Moliterni A.G.G.; Polidori G.; Spagna R. J. Appl. Cryst. 1999, 32, 115-119; (b) Altomare, A., Cascarano, G., Giacovazzo, C., Guagliardi, A., J. Appl. Cryst. 1993, 26, 343.

Sheldrick, G. M. SHELXL-97: Program for the Refinement of Crystal Structures 1997 University of Gottingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A.; MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland, 1997.

Waasmaier, D.; Kirfel, A. Acta Crystallogr. A. 1995, 51, 416.

Farrugia, L. J. Appl. Cryst. 1997, 30, 565