Crystal Structure Report for K. Goldberg

by Sarah Flowers and Werner Kaminsky

Sample Submitted by Tyler Stevens

ID – TES_018

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 12/18/14

Documentation finished: 01/02/15

Data backup accessibly through http:

URL: 	http://cad4.cpac.washington.edu/structures

Username: 	xray-user

Password: 	hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A yellow piece measuring 0.18 x 0.15 x 0.090 mm3 was mounted on a loop with oil.  Data was collected at -153oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40.00 mm and exposure time was 10 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.3 % complete to 25o in .  A total of 107,563 reflections were collected covering the indices, h = -17 to 17, k = -20 to 20, l = -19 to 19.  7,520  reflections were symmetry independent and the Rint = 0.0413 indicated that the data was better than average quality (0.07).  Indexing and unit cell refinement indicated a monoclinic lattice.  The space group was found to be P 1 21/n 1 (No.14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is of high quality and ready for publication. Table 1 summarizes the data

Figure 1 shows an ORTEP6 of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1.  Crystal data and structure refinement for tes_018_0ma.

Empirical formula 	C42 H37 I O3 P2 Rh

Formula weight 	881.47

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/n

Unit cell dimensions	a = 13.8558(8) Å	= 90°.

b = 16.7013(9) Å	= 98.532(3)°.

c = 15.9056(9) Å	 = 90°.

Volume	3640.0(4) Å3

Z	4

Density (calculated)	1.608 Mg/m3

Absorption coefficient	1.444 mm-1

F(000)	1764

Crystal size	0.18 x 0.15 x 0.09 mm3

Theta range for data collection	1.92 to 26.56°.

Index ranges	-17<=h<=17, -20<=k<=20, -19<=l<=19

Reflections collected	107563

Independent reflections	7520 [R(int) = 0.0413]

Completeness to theta = 25.00°	99.3 %

Max. and min. transmission	0.8810 and 0.7810

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7520 / 0 / 444

Goodness-of-fit on F2	1.082

Final R indices [I>2sigma(I)]	R1 = 0.0408, wR2 = 0.1124

R indices (all data)	R1 = 0.0446, wR2 = 0.1149

Largest diff. peak and hole	1.804 and -2.208 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

6 Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565