Crystal Structure Report for

Devin MacKenzie

by Paige Gannon & Werner Kaminsky

Sample Submitted by M. R. Crump

ID – TMCM_FeBrCl3_SC

X-ray Crystallography Laboratory

University of Washington

30. July 2026

Data Collection  started: 6/2/2022

Documentation finished: 6/7/2022

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

An orange shard, measuring 0.260 x 0.130 x 0.110 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.4% complete to 25o in .  A total of 5939 reflections were collected covering the indices, -17<=h<=17, -19<=k<=19, -8<=l<=8.  3091 reflections were symmetry independent and the Rint = 0.1177 indicated that the data was of slightly less than average quality (0.07).  Indexing and unit cell refinement indicated a C-centered monoclinic lattice.  The space group was found to be non-centrosymmetrical Cm (No. 8).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The most specific feature of this structure is that each of the chlorines of the Fe-anions are disordered with bromine at an individual ratio. The displacement parameters for each disordered Cl-Br pair were set to be identical and restraint also to stay positive definite. The distances to Fe were left unrestrained. As a result, the moiety formula indicates one (half) anion to be very close to resemble FeBrCl3-, a second (half) one in the asymmetric unit sees an access of bromine (FeBr1.22Cl2.78-), where the half anions are completed by symmetry. The site occupancies (x) of BrxCl1-x pairs were fitted with an errormargin between 1% to 3.7%.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C8 H22 Br2.20 Cl7.80 Fe2 N2

Formula weight 	710.29

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C m

Unit cell dimensions	a = 12.9517(15) Å	a= 90°.

b = 14.8185(16) Å	b= 98.734(6)°.

c = 6.4318(7) Å	g = 90°.

Volume	1220.1(2) Å3

Z	2

Density (calculated)	1.933 Mg/m3

Absorption coefficient	5.641 mm-1

F(000)	691

Crystal size	0.260 x 0.130 x 0.110 mm3

Theta range for data collection	2.102 to 28.348°.

Index ranges	-17<=h<=17, -19<=k<=19, -8<=l<=8

Reflections collected	5939

Independent reflections	3091 [R(int) = 0.1177]

Completeness to theta = 25.000°	99.4 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3091 / 38 / 133

Goodness-of-fit on F2	1.010

Final R indices [I>2sigma(I)]	R1 = 0.0658, wR2 = 0.1510

R indices (all data)	R1 = 0.0887, wR2 = 0.1646

Absolute structure parameter	0.11(4)

Largest diff. peak and hole	2.473 and -0.942 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,  Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565