Crystal Structure Report for K. Goldberg

by Sarah Flowers and Werner Kaminsky

Sample Submitted by Wilson Bailey

ID – WDB_3_185a

X-ray Crystallography Laboratory

University of Washington

29. July 2026

Data Collection  started: 2/12/2015

Documentation finished: 2/13/2015 (Friday!)

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A tiny yellow plate, measuring 0.1 x 0.07 x 0.01 mm3 was mounted on a loop with oil.  Data was collected at -183oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 60 seconds per frame for all sets.  The scan width was 1o.   Data collection was 99.2% complete to 25o  in .  A total of  74052 reflections were collected covering the indices, h = -17 to 17, k = -32 to 32,  l = -13 to 13.  7876 reflections were symmetry independent and the Rint = 0.1702 indicated that the data was of less than average quality (0.07).  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/c  (No. 14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

One t-butyl is disordered. One D6 C6 accompanies one molecule. The crystal was very small, thus the quality of the data was limited.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C43 H38 D6 N5 P Pt

Formula weight 	862.93

Temperature 	90(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/c

Unit cell dimensions	a = 14.227(4) Å	= 90.000°.

b = 25.622(6) Å	= 103.415(13)°.

c = 10.659(3) Å	 = 90.000°.

Volume	3779(2) Å3

Z	4

Density (calculated)	1.517 Mg/m3

Absorption coefficient	3.792 mm-1

F(000)	1720

Crystal size	0.10 x 0.07 x 0.01 mm3

Theta range for data collection	2.12 to 26.72°.

Index ranges	-17<=h<=17, -32<=k<=32, -13<=l<=13

Reflections collected	74052

Independent reflections	7876 [R(int) = 0.1702]

Completeness to theta = 25.00°	99.2 %

Max. and min. transmission	0.9631 and 0.7029

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7876 / 54 / 485

Goodness-of-fit on F2	0.983

Final R indices [I>2sigma(I)]	R1 = 0.0791, wR2 = 0.1520

R indices (all data)	R1 = 0.1843, wR2 = 0.1937

Largest diff. peak and hole	3.437 and -4.054 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565