Crystal Structure Report for K Goldberg

by Maike Blakely and Werner Kaminsky

Sample Submitted by Zuzana Culakova

ID – ZCII_74

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 1/6/2017

Documentation finished: 1/13/2017

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A yellow? prism, measuring 0.26 x 0.05 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 180 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 96.1% complete to 25o  in .  A total of  129012 reflections were collected covering the indices, -18<=h<=18, -29<=k<=29, -22<=l<=22.  6335 reflections were symmetry independent and the Rint = 0.0892 indicated that the data was appropriate.  Indexing and unit cell refinement indicated after many attempts a primitive orthorhombic lattice.  The space group was found to be P n m a  (No. 62).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The asymmetric unit shows two half molecules, completed through mirror symmetry on c. One of the two halfs is in addition disordered, with Ir at two different positions (full molecule disorder). One CH2Cl2 (disordered) and a triply disordered OTF complete the unit. The hydrides were placed in a likely geometry.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. One completed molecule shown. Disorder and solvent omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C28 H46 Cl2 F3 Ir O5 P2 S

Formula weight 	876.75

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P n m a

Unit cell dimensions	a = 15.492(5) Å	= 90°.

b = 24.393(5) Å	= 90°.

c = 18.535(5) Å	 = 90°.

Volume	7004(3) Å3

Z	8

Density (calculated)	1.663 Mg/m3

Absorption coefficient	4.166 mm-1

F(000)	3504

Crystal size	0.26 x 0.05 x 0.05 mm3

Theta range for data collection	1.38 to 25.35°.

Index ranges	-18<=h<=18, -29<=k<=29, -22<=l<=22

Reflections collected	129012

Independent reflections	6335 [R(int) = 0.0892]

Completeness to theta = 25.00°	96.1 %

Max. and min. transmission	0.8188 and 0.4105

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6335 / 321 / 578

Goodness-of-fit on F2	1.203

Final R indices [I>2sigma(I)]	R1 = 0.0689, wR2 = 0.1401

R indices (all data)	R1 = 0.0787, wR2 = 0.1446

Largest diff. peak and hole	1.812 and -2.206 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565