Crystal Structure Report for K. Goldberg

by Maike Blakely & Werner Kaminsky

Sample Submitted by Zoha Syed

ID – ZS_02_052

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 1/27/2017

Documentation finished: 1/30/2017

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A red prism, measuring 0.50 x 0.25 x 0.25 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 10 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.5% complete to 25o  in .  A total of  127051 reflections were collected covering the indices, -13<=h<=13, -32<=k<=32, -16<=l<=16.  7513 reflections were symmetry independent and the elevated Rint = 0.0332 reflects the good quality of the crystal. Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21/c  (No. 14).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Hydrogens omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula                		C19 H27 Cl2 I2 Ir N2 O3

Formula weight                    		848.32

Temperature                       		100(2) K

Wavelength                        		0.71073 Å

Crystal system, space group       		Monoclinic,  P 21/n

Unit cell dimensions              		a = 9.3446(11) Å   	alpha = 90°

b = 22.696(3) Å    	beta = 101.095(6) °

c = 11.6304(14) Å   	gamma = 90°

Volume                            			2420.5(5) Å3

Z, Calculated density             		4,  2.328 Mg/m3

Absorption coefficient            		8.310 mm-1

F(000)                            			1584

Crystal size                      			0.500 x 0.250 x 0.200 mm

Theta range for data collection   		1.795° to 30.754°

Limiting indices                  		-13<=h<=13, -32<=k<=32, -16<=l<=16

Reflections collected / unique    		127051 / 7513 [R(int) = 0.0332]

Completeness to theta = 25.242  		99.5 %

Refinement method                 		Full-matrix least-squares on F2

Data / restraints / parameters    		7513 / 3 / 275

Goodness-of-fit on F2            		1.013

Final R indices [I>2sigma(I)]     		R1 = 0.0240, wR2 = 0.0525

R indices (all data)              		R1 = 0.0277, wR2 = 0.0542

Extinction coefficient            		0.00016(2)

Largest diff. peak and hole       		1.522 and -2.674 e. Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2013) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3-8.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565