Crystal Structure Report for M. Larsen

by Werner Kaminsky

Sample ID – CCB1_91

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 7/24/2024

Documentation finished: 7/29/2024

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A colorless shard, measuring 0.10 x 0.07 x 0.01 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation, equipped with a Miracol X-ray optical collimator.

Crystal-to-detector distance was 40 mm and exposure time was 120 seconds per frame for all sets.  The scan width was 1o.   Data collection was 96.0% complete to 24.404o in .  A total of  3099 merged reflections were collected covering the indices, -13<=h<=13, -8<=k<=8, -13<=l<=14.  1537 reflections were symmetry independent and the Rint = 0.1725 indicated that the data was of lower than average quality (0.07) due to twinning.  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be x xx  (No.xx).

The data appeared multiply twinned 1) via 180 degrees approximately about   (1 0 0),  2) 7 degrees rotation about [-0.37 -0.47 1] (CELL_NOW) and after multi-domain integration (SAINT, SADABS within the APEX2 software package by Bruker) the data was merged utilizing twinabs.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL. Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

In addition to the above twiinin and due to the similarity in length of the a and b axis, a pseudo merohedral twin was applied to the refinement with twin matrix (0  0  1,  0 -1  0,  1  0  0). With so many twin components, the data could only be of limited quality.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C11 H14 N2 O

Formula weight 	190.24

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21/n

Unit cell dimensions	a = 12.008(5) Å	a= 90°.

b = 7.222(3) Å	b= 111.702(17)°.

c = 12.070(5) Å	g = 90°.

Volume	972.6(7) Å3

Z	4

Density (calculated)	1.299 Mg/m3

Absorption coefficient	0.085 mm-1

F(000)	408

Crystal size	0.100 x 0.070 x 0.010 mm3

Theta range for data collection	1.816 to 24.404°.

Index ranges	-13<=h<=13, -8<=k<=8, -13<=l<=14

Reflections collected	3099

Independent reflections	1537 [R(int) = 0.1725]

Completeness to theta = 24.404°	96.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1537 / 84 / 130

Goodness-of-fit on F2	1.050

Final R indices [I>2sigma(I)]	R1 = 0.1705, wR2 = 0.3474

R indices (all data)	R1 = 0.2323, wR2 = 0.3796

Largest diff. peak and hole	0.771 and -0.591 e.Å-3

Sheldrick, G. M. (2005). CELL_NOW. University of Goettingen, Germany.

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick, G. M. (2007). TWINABS. University of Goettingen, Germany.

(a) Sheldrick GM. (2008) A short history of SHELX. Acta Cryst. A64, 112-122.

(b) Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,  Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. C71, 3–8

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565