Crystal Structure Report for

Sei-Hum Jang

by Werner Kaminsky

Sample Submitted by Francis Lin

ID – Francis_27B

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 1/12/2021

Documentation finished: 1/15/2021

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A black prism, measuring 1.00 x 0.20 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 60 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 98.1% complete to 25o  in .  A total of  30189 merged reflections were collected covering the indices, -28<=h<=27, -69<=k<=69, -16<=l<=16.  15251 reflections were symmetry independent and the Rint = 0.1747 indicated that the data was of appropriate quality.  Indexing and unit cell refinement indicated a C-centered monoclinic lattice.  The space group was found to be C 2/c  (No. 15).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The chromophore is accompanied by some liquid solvent inside infinite cavities along the c-axis, the contribution of which to the diffraction pattern, except for a (half) chloroform that was located on the inversion center of the lattice, was removed with SQUEEZE. In addition one side chain was disordered.

The structure is of good quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 30% probability level. Disorder and SQUEEZED solvent omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C173 H189 Cl3 F8 N16 O4 S8 Se2

Formula weight 	3229.14

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C 2/c

Unit cell dimensions	a = 23.525(6) Å	a= 90°.

b = 58.196(14) Å	b= 111.813(13)°.

c = 13.819(3) Å	g = 90°.

Volume	17565(7) Å3

Z	4

Density (calculated)	1.221 Mg/m3

Absorption coefficient	0.626 mm-1

F(000)	6760

Crystal size	1.000 x 0.200 x 0.050 mm3

Theta range for data collection	1.400 to 25.027°.

Index ranges	-28<=h<=27, -69<=k<=69, -16<=l<=16

Reflections collected	30189

Independent reflections	15251 [R(int) = 0.1747]

Completeness to theta = 25.000°	98.1 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	15251 / 1227 / 977

Goodness-of-fit on F2	1.124

Final R indices [I>2sigma(I)]	R1 = 0.1899, wR2 = 0.3650

R indices (all data)	R1 = 0.3633, wR2 = 0.4439

Largest diff. peak and hole	0.853 and -0.633 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565