Crystal Structure Report for

Sei-Hum Jang

by Werner Kaminsky

Sample Submitted by Francis Lin

ID – Cranfis_45_1

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data Collection  started: 4/26/2021

Documentation finished: 5/17/2021

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A black plate, measuring 0.30 x 0.20 x 0.05 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per frame for all sets.  The scan width was 0.75o.   Data collection was 99.4% complete to 24.257o in .  A total of  29289 merged reflections were collected covering the indices, -15<=h<=15, -25<=k<=26, 0<=l<=35, Rint = 0.1969.  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P1  (No. 2).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The chromophore crystals exhibit extensive disorder in their sidechains and despite good mosaicity and long exposure time did not diffract effectively beyond a resolution of 1.1. In addition, the crystals appeared twinned via twin law (-1 0  0,  0 -1 0,  0 -1  1) and contained disordered solvent requiring application of SQUEEZE to remove the solvent's contribution to the diffraction pattern. The proposed structure sees one half of the chromophore sulfonated, the other with a Se on the outside sulfur position in the vicinity of oxygen. From the refinement of displacement parameters, the presence of a more strongly scattering Se was verified but distributed as 1:1 disorder to all outside sulfur positions.

The structure is problematic statistical quality, but probably publishable when appropriate comments are given. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 15% probability level. Disorder and SQUEEZED solvent omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C86 H94 F4 N8 O2 S4 Se

Formula weight 	1554.89

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 13.6110(13) Å	a= 70.204(8)°.

b = 23.275(3) Å	b= 84.824(7)°.

c = 30.960(4) Å	g = 80.863(7)°.

Volume	9104(2) Å3

Z	4

Density (calculated)	1.134 Mg/m3

Absorption coefficient	0.559 mm-1

F(000)	3264

Crystal size	0.300 x 0.200 x 0.050 mm3

Theta range for data collection	1.343 to 24.257°.

Index ranges	-15<=h<=15, -25<=k<=26, 0<=l<=35

Reflections collected	29289

Independent reflections	29289 [R(int) = 0.1969]

Completeness to theta = 24.257°	99.4 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	29289 / 3791 / 2084

Goodness-of-fit on F2	1.024

Final R indices [I>2sigma(I)]	R1 = 0.2465, wR2 = 0.4422

R indices (all data)	R1 = 0.5123, wR2 = 0.5329

Largest diff. peak and hole	0.739 and -0.603 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565