Crystal Structure Report for B. Cossairt

by Sarah Flowers & Werner Kaminsky

Sample Submitted by Dylan Gary

ID – dg_052615

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

Data Collection  started: 5/26/2015

Documentation finished: 7/24/2015

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

A yellow piece, measuring 0.19 x 0.15 x 0.15 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 60 mm and exposure time was 60 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.7 % complete to 25o  in .  A total of  254930 reflections were collected covering the indices, h = -28 to 28, k = -29 to 29,  l = -51 to 51.  80008 reflections were symmetry independent and the Rint = 0.0708 indicated that the data was of average quality.  Indexing and unit cell refinement indicated a triclinic lattice.  The space group was found to be P1 (No. 2).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

Solvent analysis discovered two two distinct voids filled with diethylether and related contribution to the diffraction pattern was removed with SQEEZE

With the size of the molecule comes implicitely the possibility of disorder, which may have contributed to larger than expected positive as well as negative rest electron densities around the indium atoms, estimated to about 2% which also leeds to an increased R1 value. Possible is also some chemical inhomogeneity due to the inclusion of  water by exposure to ambient humidity, the process of which was difficult to monitor for completion. Some disorder of the phenyls was treated explicitly as some inter molecular ‘squeezing’ occurs. As a result of the large molecular size (11.7 kD) and strong scattering of the In-P-cluster, carbon atoms were weekly represented in the data, requiring DELU (In-O-C) and ISOR (O, C) restraints. In addition, the general geometry of the organic molecules was linked via SAME commands. The structure is of high quality and ready for publication. Table 1 summarizes the data collection details.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 25% probability level. Disorder omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C408 H359 In37 O103 P20

Formula weight 	11777.67

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P -1

Unit cell dimensions	a = 23.5228(11) Å	= 84.905(3)°.

b = 24.1862(12) Å	= 88.006(3)°.

c = 43.0370(19) Å	 = 63.079(3)°.

Volume	21744.9(18) Å3

Z	2

Density (calculated)	1.799 Mg/m3

Absorption coefficient	2.067 mm-1

F(000)	11488

Crystal size	0.190 x 0.150 x 0.150 mm3

Theta range for data collection	1.634 to 25.472°.

Index ranges	-28<=h<=28, -29<=k<=29, -51<=l<=51

Reflections collected	254930

Independent reflections	80008 [R(int) = 0.0708]

Completeness to theta = 25.000°	99.7 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.7468 and 0.6948

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	80008 / 34585 / 4771

Goodness-of-fit on F2	1.205

Final R indices [I>2sigma(I)]	R1 = 0.1283, wR2 = 0.3359

R indices (all data)	R1 = 0.1935, wR2 = 0.3771

Largest diff. peak and hole	7.109 and -1.973 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

A. Spek, J. Appl. Cryst. (2003), 36, 7-13; P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565