Crystal Structure Report for B Cossairt

by Werner Kaminsky

Sample Submitted by D Henckel

ID – DH_184

X-ray Crystallography Laboratory

University of Washington

31. July 2026

Data backup accessibly through http:

URL: 	http://cad4.cpac.washington.edu/structures

Username: 	xray-user

Password: 	hkl-data

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures. Even I  have to pay for my own structures for my research.

An orange plate, measuring 0.10 x 0.10 x 0.02 mm3 was mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 60 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 100% complete to 25o  in .

The data appeared twinned (CELL_NOW) and after  multi-domain integration (SAINT, SADABS within the APEX2 software package by Bruker.) and merging (twinabs) a total of  9984 (merged) reflections covered the indices, h = -38 to 02, k = -10 to 38,  l = -22 to 20.  3421 reflections were symmetry independent and the Rint = 0.0746 indicated that the data was of  average quality (0.07).  Indexing and unit cell refinement indicated a rhombohedral lattice.  The space group was found to be R3 c   (No.167).

Solution by direct methods (SHELXS, SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL97., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The structure is very similar to that of the equivalent Mn-compound with slightly different site occupancies of the disordered ClO4- and water.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder anions and solvent omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C54 H96 Cd Cl5 Co3 N24 O32

Formula weight 	2059.99

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Trigonal

Space group 	R -3 c

Unit cell dimensions	a = 28.981(3) Å	= 90°.

b = 28.981(3) Å	= 90°.

c = 16.838(4) Å	 = 120°.

Volume	12247(3) Å3

Z	6

Density (calculated)	1.676 Mg/m3

Absorption coefficient	1.117 mm-1

F(000)	6348

Crystal size	0.10 x 0.10 x 0.02 mm3

Theta range for data collection	2.43 to 28.46°.

Index ranges	-38<=h<=0, -10<=k<=38, -22<=l<=20

Reflections collected	9984

Independent reflections	3421 [R(int) = 0.0746]

Completeness to theta = 25.00°	100.0 %

Max. and min. transmission	0.9780 and 0.8965

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3421 / 83 / 261

Goodness-of-fit on F2	1.190

Final R indices [I>2sigma(I)]	R1 = 0.0789, wR2 = 0.1311

R indices (all data)	R1 = 0.1306, wR2 = 0.1474

Largest diff. peak and hole	0.505 and -0.430 e.Å-3

Sheldrick, G. M. (2005). CELL_NOW. University of Goettingen, Germany.

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

Sheldrick, G. M. (2007). TWINABS. University of Goettingen, Germany.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565