Crystal Structure Report for S Jenekhe

by Werner Kaminsky

Sample Submitted by Xiaomei Ding

ID – xiaomei_dno

X-ray Crystallography Laboratory

University of Washington

28. July 2026

Data Collection  started:  5/15/2019

Documentation finished:  5/24/2019

Data backup accessibly through http:

URL: http://cad4.cpac.washington.edu/structures

W.Kaminsky: tel. (206) 543 7585

(x-ray lab):     tel. (206) 543 0210

Email: kaminsky@chem.washington.edu

Understanding crystallographic information is not trivial. If you discuss a structure in a publication, please let the crystallographers proof-read the final draft of that manuscript before you submit it.

For many structures it is true that crystallography is an intellectual performance (like synthesis or elucidation of mechanisms) and not a routine job. In these cases, particularly when the structures contribute significantly to the content of the publication, the crystallographers should be co-authors. Do not think this is not necessary because you pay for structures.

A black plate, stable in paraffine oil for maximal 10 seconds after removal from growth solution, measuring 0.60 x 0.15 x 0.07 mm3 was (very quickly) mounted on a loop with oil.  Data was collected at -173oC on a Bruker APEX II single crystal X-ray diffractometer, Mo-radiation.

Crystal-to-detector distance was 40 mm and exposure time was 30 seconds per frame for all sets.  The scan width was 0.5o.   Data collection was 99.9% complete to 25o  in .  A total of  16581 merged reflections were collected covering the indices, -18<=h<=18, -27<=k<=27, -33<=l<=33.  16569 reflections were symmetry independent and the Rint = 0.0658 indicated that the data was of good quality (0.07).  Indexing and unit cell refinement indicated a primitive monoclinic lattice.  The space group was found to be P 21  (No. 4).

The data was integrated and scaled using SAINT, SADABS within the APEX2 software package by Bruker.

The contribution to the diffraction pattern of about 16 disordered CH2Cl2 solvent in the unit cell inside infinite channels roughly along the a-axis was removed with SQUEEZE

Solution by direct methods (SHELXT or SIR97) produced a complete heavy atom phasing model consistent with the proposed structure. The structure was completed by difference Fourier synthesis with SHELXL., Scattering factors are from Waasmair and Kirfel. Hydrogen atoms were placed in geometrically idealised positions and constrained to ride on their parent atoms with C---H distances in the range 0.95-1.00 Angstrom. Isotropic thermal parameters Ueq were fixed such that they were 1.2Ueq of their parent atom Ueq for CH's and 1.5Ueq of their parent atom Ueq in case of methyl groups. All non-hydrogen atoms were refined anisotropically by full-matrix least-squares.

The asymmetric unit contains two chromopohores, one of which is slightly disordered. The structure is enantiomorphically twinned, with refined Flack parameter of  0.43(17) and mimics pseudo P21/a symmetry.

The structure is of high quality and ready for publication. Table 1 summarizes the data collection details. Figure 1 shows an ORTEP of the asymmetric unit.

Figure 1. ORTEP of the structure with thermal ellipsoids at the 50% probability level. Disorder and solvent omitted for clarity.

Table 1: Crystallographic data for the structures provided.

Empirical formula 	C96 H86 O4 S4

Formula weight 	1431.88

Temperature 	100(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P 21

Unit cell dimensions	a = 15.0487(8) Å	= 90°.

b = 21.7183(12) Å	= 95.097(3)°.

c = 26.7134(13) Å	 = 90°.

Volume	8696.3(8) Å3

Z	4

Density (calculated)	1.094 Mg/m3

Absorption coefficient	0.157 mm-1

F(000)	3032

Crystal size	0.600 x 0.150 x 0.070 mm3

Theta range for data collection	1.499 to 25.494°.

Index ranges	-18<=h<=18, -27<=k<=27, -33<=l<=33

Reflections collected	16581

Independent reflections	16569 [R(int) = 0.0658]

Completeness to theta = 25.000°	99.9 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	16569 / 1181 / 1884

Goodness-of-fit on F2	1.016

Final R indices [I>2sigma(I)]	R1 = 0.0728, wR2 = 0.1800

R indices (all data)	R1 = 0.1099, wR2 = 0.2032

Absolute structure parameter	0.43(17)

Largest diff. peak and hole	0.655 and -0.414 e.Å-3

Bruker (2007) APEX2 (Version 2.1-4), SAINT (version 7.34A), SADABS (version 2007/4), BrukerAXS Inc, Madison, Wisconsin, USA.

(a) A. Spek, J. Appl. Cryst. (2003), 36, 7-13;

(b) P. van der Sluis & A. L. Spek, Acta Cryst. (1990). A46, 194-201.

(c) Spek, A. L. (2009). Acta. Cryst. D65, 148-155.

Sheldrick GM. (2015) SHELXT - Integrated space-group and crystal-structure determination. Acta Cryst. A71, 3-8.

(a) Altomare A, Burla C, Camalli M, Cascarano G L, Giacovazzo C, Guagliardi A,   Moliterni AGG, Polidori G, Spagna R. (1999) SIR97: a new tool for crystal structure determination and refinement Journal of Applied Crystallography, 32, 115-119.

(b) Altomare A, Cascarano G L, Giacovazzo C, Guagliardi A. (1993) Completion and refinement of crystal structures with SIR 92. Journal of Applied Crystallography, 26, 343-350.

(a) Sheldrick GM. (1997) SHELXL-97, Program for the Refinement of Crystal Structures. University of Göttingen, Germany.

(b) Sheldrick GM. (2015) Crystal structure refinement with SHELXL. Acta Cryst. (2015). C71, 3–8

Mackay, S.; Edwards, C.; Henderson, A.; Gilmore, C.; Stewart, N.; Shankland, K.; Donald, A. (1997) MaXus: a computer program for the solution and refinement of crystal structures from diffraction data. University of Glasgow, Scotland,.

Waasmaier, D.; Kirfel, A. (1995) New Analytical Scattering Factor Functions for Free Atoms and Ions. Acta Crystallographica A., 51, 416-430.

Farrugia LJ. (1997) Ortep-3 for Windows. Journal of Applied Crystallography, 30, 565